## Slide 1: 2nd harmonic RF perpendicular biased cavity update
C.Y. Tan, W. Pellico, G. Romanov, R. Madrak,
and D. Wildman
04 Apr 2014

## Slide 2: Proposed cavity.
Ferrite disk: 380 mm outer diam., 230 mm inner diam., 25 mm thickness
BeO disk: 380 mm outer diam., 230 mm inner diam., 5 mm thickness
490
70
40
200
220
390
Ferrite
BeO
solenoid not shown here

## Slide 3: Some possible parameters
Tuning range 76.7 − 107 MHz.
Gap voltage. 100 kV per cavity.
Ramp profile determines losses in the garnet.

## Slide 4: CST Model (done by G. Romanov)
Complete cavity model with magnetic field generated by solenoid
Solenoid coil

## Slide 5
R110
R205
190 mm
Yoke, steel 1008
Coil, 12 turns
Water cooling channels, 10x5 mm
Ferrite G810, R=190 mm, r=115 mm, l=25 mm
Ceramic AlN, l=5mm
230 mm
90 mm
20 mm
This is old picture, not properly scaled. But the marked dimensions are current.
Ferrite tuner details

## Slide 6: Static field distribution in ferrite
Separate solenoid model
Complete cavity model
Field non-uniformity is about 25-30%

## Slide 7: Suppression of fields with steel insert.
Yoke
Coil
Ferrite
Copper drift tube
Steel 1008 insert
Radial distribution of H field at tuner median plane. H field on the axis can be as high as 85 kA/m. With steel drift tube it is suppressed.

## Slide 8: RF magnetic field distribution in ferrite and losses
f=75.6 MHz
These power losses spikes are not real. They are due to the singularity of low frequency mesh that is used for thermal simulations

## Slide 9: Tuning curves
Chart: Solenoid current, Ampere·turns
| 30000.0 | 24000.0 | 18000.0 | 15600.0 | 13200.0 | 12000.0 | 10800.0 | 9600.0 | 8400.0 | 7200.0 | 6000.0 | 4800.0 | 4500.0 | 4440.0 | 100.0
 | 112.55 | 109.78 | 105.56 | 103.18 | 100.14 | 98.31 | 96.2 | 93.72 | 90.78 | 87.27 | 82.95 | 77.52 | 75.92 | 75.6
Conversion of the solenoid current to the equivalent uniform field. We can continue to use uniform magnetization – the results are very close.

## Slide 10: Thermal analysis
AlN cooling disks. Thermal losses in the ferrite are 14 kW for V=100 kV. Max T ≈ 75°C with cooling water temperature of 25°C.
Chart: Saturation magnetization, Gauss
| 219.0 | 400.0 | 650.0 | 800.0 | 1000.0 | 1030.0 | 1200.0 | 1210.0 | 1400.0 | 1510.0
Cuire, °C | 100 | 130 | 175 | 200 | 210 | 215 | 230 | 230 | 245 | 255
Curie temperature

## Slide 11: Mulitpacting with maximum solenoidal field
Range: up to 2.5 % of nominal field level
Location of multipacting
Exponential growth of particle number

## Slide 12: Mulitpacting without solenoidal field
Range: up to 1 % of nominal field level
Exponential growth of particle number
Location of multipacting

## Slide 13: Magnetic permeability (Gyrotropic model)

## Slide 14: Measuring AL400 (R. Madrak and D. Wildman)

## Slide 15: Measured losses
Chart: Measured Losses Vs Solenoid Bias
| 0.0 | 10.0 | 12.0 | 14.0 | 16.0 | 18.0 | 22.0 | 24.0 | 26.0 | 28.0 | 30.0 | 32.0 | 34.0 | 36.0 | 38.0 | 40.0 | 42.0 | 44.0 | 46.0 | 48.0 | 50.0 | 52.0 | 54.0 | 56.0 | 58.0 | 60.0 | 65.0 | 70.0 | 75.0 | 80.0 | 90.0 | 100.0
76 MHz | 7.05 | 3.26 | 2.3604 | 1.6412 | 1.1098 | 0.7285 | 0.2846 | 0.1657 | 0.0883 | 0.0469 | 0.0254 | 0.0173 | 0.0115 | 0.0121 | 0.0071 | 0.0027 | 0.0058 | 0.0007 | -0.0031 | 0.0042 | 0.0009 | 0 | 0.0007 | 0.0038 | 0.0002 | -0.0045 | -0.0022 | 0.0038 | 0.0001 | 0.0014 | -0.0013 | 0.0001
106 MHz | 7.09 | 7.11 | 6.326 | 4.7395 | 3.1825 | 2.0072 | 0.701 | 0.397 | 0.2067 | 0.1161 | 0.0544 | 0.0405 | 0.0311 | 0.0253 | 0.0211 | 0.017 | 0.0198 | 0.0138 | 0.0117 | 0.0149 | 0.0051 | 0.0122 | 0.0048 | 0.01 | 0.017 | 0.0136 | 0.0067 | 0.0085 | 0.0055 | 0.0043 | -0.0058 | 0.0029
53 MHz | 7.31 | 2.295 | 1.681 | 1.2418 | 0.9119 | 0.6352 | 0.2705 | 0.16 | 0.0873 | 0.0517 | 0.0296 | 0.0127 | 0.0157 | -0.0009 | 0.0002 | 0.0047 | 0.0039 | 0 | -0.0025 | 0.0015 | -0.0068 | -0.0053 | -0.0055 | -0.0005 | -0.0004 | -0.0046 | -0.0057 | -0.01 | -0.0071 | -0.0006 | -0.003 | -0.0037
method looks at s11 and from there calculate the loss in the garnet.
This number will scale with the length of the garnet.

## Slide 16: Model in ADS used to calculate μ’ from s11 phase data

## Slide 17: Fits to the s11 phase data

## Slide 18: Measured μ
Chart: Mu and Losses, 76 MHz
| 0.0 | 10.0 | 12.0 | 14.0 | 16.0 | 18.0 | 22.0 | 24.0 | 26.0 | 28.0 | 30.0 | 32.0 | 34.0 | 36.0 | 38.0 | 40.0 | 42.0 | 44.0 | 46.0 | 48.0 | 50.0 | 52.0 | 54.0 | 56.0 | 58.0 | 60.0 | 65.0 | 70.0 | 75.0 | 80.0 | 90.0 | 100.0
Mu | 6.5016 | 6.89 | 6.4592 | 5.9173 | 5.3674 | 4.856 | 4.0302 | 3.7102 | 3.438 | 3.2149 | 3.0287 | 2.871 | 2.7367 | 2.6271 | 2.5201 | 2.4383 | 2.3582 | 2.2861 | 2.2163 | 2.1612 | 2.1079 | 2.058 | 2.014 | 1.9702 | 1.9307 | 1.8925 | 1.8054 | 1.7328 | 1.666 | 1.6095 | 1.5091 | 1.427
Losses | 7.05 | 3.26 | 2.3604 | 1.6412 | 1.1098 | 0.7285 | 0.2846 | 0.1657 | 0.0883 | 0.0469 | 0.0254 | 0.0173 | 0.0115 | 0.0121 | 0.0071 | 0.0027 | 0.0058 | 0.0007 | -0.0031 | 0.0042 | 0.0009 | 0 | 0.0007 | 0.0038 | 0.0002 | -0.0045 | -0.0022 | 0.0038 | 0.0001 | 0.0014 | -0.0013 | 0.0001
Chart: Mu and Losses, 106 MHz
| 0.0 | 10.0 | 12.0 | 14.0 | 16.0 | 18.0 | 22.0 | 24.0 | 26.0 | 28.0 | 30.0 | 32.0 | 34.0 | 36.0 | 38.0 | 40.0 | 42.0 | 44.0 | 46.0 | 48.0 | 50.0 | 52.0 | 54.0 | 56.0 | 58.0 | 60.0 | 65.0 | 70.0 | 75.0 | 80.0 | 90.0 | 100.0
Mu | 4.0824 | 5.0713 | 5.499 | 5.5686 | 5.2727 | 4.8208 | 3.9447 | 3.6016 | 3.3136 | 3.0843 | 2.8965 | 2.7404 | 2.6114 | 2.5077 | 2.4076 | 2.3334 | 2.2605 | 2.1967 | 2.136 | 2.0892 | 2.0428 | 2.0015 | 1.9659 | 1.9316 | 1.8994 | 1.8708 | 1.8059 | 1.7555 | 1.7106 | 1.6748 | 1.6128 | 1.566
Losses | 7.09 | 7.11 | 6.326 | 4.7395 | 3.1825 | 2.0072 | 0.701 | 0.397 | 0.2067 | 0.1161 | 0.0544 | 0.0405 | 0.0311 | 0.0253 | 0.0211 | 0.017 | 0.0198 | 0.0138 | 0.0117 | 0.0149 | 0.0051 | 0.0122 | 0.0048 | 0.01 | 0.017 | 0.0136 | 0.0067 | 0.0085 | 0.0055 | 0.0043 | -0.0058 | 0.0029
recall μe = μ’ – iμ’’.
Back of the envelope requires
μmax/μmin = (fmax/fmin)2 = (106/76) 2≈ 2.
Sims say ratio is 2.5, then if μmin=1.5, then μmax=1.5×2.5 = 3.75
μ’
prop to μ’’
3.75
24
-0.4 dB loss @ μ’=3.75
s11 = (Pin - Pref )/Pin = 1-Pref/Pin.
In dB = 10 Log10(1- Pref/Pin)
≈10(-0.43 x – 0.21 x2)
Tan[δ] = μ’’/μ’=1/Q

## Slide 19: Todo (partial list) to be discussed
Check that solenoid can be built.
  PS for solenoid -- kA
Coupler?
PA?
Dimensions OK?
Impedance of cavity? Shunt impedance > 1 MΩ?
How to incorporate μ measurements into simulations?