## Slide 1: Design modifications. Reproducing of Al800 measurements in CST MWS.
January 14, 2015
G.Romanov, Y.Terechkine

## Slide 2
  Design modifications.
      Cooling cylinder.
      Cooling cylinder + taper.
      Bill Pellico’s proposal.
Reminder of the material unknowns.
Simulations of Robyn’s measurements of Al800 garnet.
    Model of the set up.
    Magnetostatic simulations.
    Simulation with original AL800 parameters.
    Dielectric constant of Al800.
    Garnet B(H) curve.
    Fitting B(H) for Al800.
    Conclusion on B(H), ΔH and ε of the Al800 garnet.
Content

## Slide 3
Design modifications
Ferrite: L = 110 mm, ΔH = 31 Oe at 9.4 GHz, tanδ_E = 0.0002
H field
H field
H field
Volume losses
Volume losses
Volume losses
F, MHz | 76.2 | 78.15 | 77.18
Peak losses in the ferrite at V=100 kV | 49 | 52 | 55
Base
Cooling cylinder
Taper +
Cooling cylinder

## Slide 4
Bill’s proposal (speculation, no simulations yet)
Using copper cooling cylinders instead of beryllium disks in
the original design. It should work in general.
Original design
Variant 1.
Overheating of the central part is possible.
Variant 2.
The gap will be a source of field non-uniformity.
This variant is actually what we are considering now.

## Slide 5
α = γΔH/4πf =>
Reminder
In CST the loss mechanism within ferrites at RF frequencies is associated with precessional
damping. This damping is commonly described by a damping coefficient, commonly referred
to as α in the Landau–Lifshitz equation. It can be introduced directly or using the half–power ferromagnetic resonance (FMR) linewidth ΔH. These two quantities are related to each other by
where f is the frequency at which the swept field linewidth is measured and γ= 2.8 GHz/kOe, ω – operating frequency.
ΔH – uniform spin-precession resonance
ΔHk – spin-wave resonance
ΔHeff – effective linewidth
Which ΔH to use?
Try to get answer from the measurements.
“Domen”, ΔH=31 Oe, f=9.4 GHz
Thermal losses ≈ 4 kW at 100 kV
“Shapiro”, ΔH=1.5 Oe, f=9.4 GHz
Thermal losses ≈2 kW at 100 kV

## Slide 6
CST model of the Al800 set-up
Outer conductor ID: 3.027:
Inner conductor OD: 0.625”
Garnet OD/ID 3”, 0.65”
Shorted end
This is a thin piece
of copper with
BNC connectors
with BNC connectors
as pickups
Sketch of the set-up from Robyn
CST model
Solenoid coil,
112 turns
Solenoid yoke,
CMD ferrite
Antenna
Copper cavity
Al800 garnet

## Slide 7
Magnetostatic solver
Chart: I_sol, A
| 35.076999999999998 | 39.987780000000001 | 44.94867 | 50.21022 | 55.171109999999999 | 60.131999999999998 | 65.493769999999998 | 70.153999999999996 | 75.265219999999999 | 80.226109999999991 | 85.136890000000008 | 90.14788999999999 | 95.208999999999989 | 99.969450000000009
Robyn's formula | 262.2707 | 298.9886 | 336.0812 | 375.4218 | 412.5144 | 449.607 | 489.6969 | 524.5415 | 562.758 | 599.8506 | 636.5685 | 674.0358 | 711.8777 | 747.4716
CST sim. | 233.7596 | 311.8848 | 390.3617 | 468.4994 | 546.4486 | 624.4984 | 702.8622 | 781.1005
Robyn: In empty resonator H_int (Oe) = 7.477·I_sol(A)
H field
|H| field
In this simuations both yoke CMD ferrite and Al800 garnet are non-linear. But CMD can be replaced in by material with fixed µ = 2000 without compromising accuracy of simulations (Y. Terechkine, verified by CST simulations).
along y = 0.4”

## Slide 8
Simulations of Al800 set-up with original G810 parameters
dH = 40 Oe at 9.4 GHz; Ms = 810 Oe; ε = 14.4, 13.86 and 10.4; tanδ_e=0.0002
Chart: I_sol, A
| 35.076999999999998 | 39.987780000000001 | 44.94867 | 50.21022 | 55.171109999999999 | 60.131999999999998 | 65.493769999999998 | 70.153999999999996 | 75.265219999999999 | 80.226109999999991 | 85.136890000000008 | 90.14788999999999 | 95.208999999999989 | 99.969450000000009
Exper. | 73.8 | 81.65 | 87.85 | 93.633 | 98.357 | 102.457 | 106.394 | 109.428 | 112.481 | 115.163 | 117.607 | 119.914 | 122.045 | 123.917
CST, eps=10.4 | 76.195 | 83.025 | 88.974 | 94.133 | 98.445 | 102.26 | 105.69 | 108.79 | 111.61 | 114.2 | 116.58 | 118.78 | 120.83 | 122.745 | 124.5
CST, eps=13.86 | 66.148 | 72.236 | 77.46 | 85.638 | 91.925 | 97.075 | 101.39 | 106.75 | 108.37
    Since electrical field is strong in the ferrite, impact of ε is significant. Upper 123 MHz is dominated by ε, since µ ≤ 2.
    Assume that ε drops from static value of 13.8 to 10.4-10.5 and remains constant in 70-123 MHz interval. The
    tanδ_e=0.0002 is constant as well.
TRIUMF

## Slide 9
Chart: I_sol, A
| 35.076999999999998 | 39.987780000000001 | 44.94867 | 50.21022 | 55.171109999999999 | 60.131999999999998 | 65.493769999999998 | 70.153999999999996 | 75.265219999999999 | 80.226109999999991 | 85.136890000000008 | 90.14788999999999 | 95.208999999999989 | 99.969450000000009
Exper. | 73.8 | 81.65 | 87.85 | 93.633 | 98.357 | 102.457 | 106.394 | 109.428 | 112.481 | 115.163 | 117.607 | 119.914 | 122.045 | 123.917
CST sim. | 74.4 | 94.82 | 106.63 | 115.4 | 123.89
Chart: H, A/m
| 0 | 801 | 1197.94 | 2546.48 | 7957.75 | 15915.5 | 31831 | 48438.5 | 63662 | 95876.5 | 135336 | 175539 | 214247
Y.T. analit. | 0 | 0.05 | 0.07 | 0.08 | 0.09 | 0.1 | 0.12 | 0.14 | 0.16 | 0.2 | 0.25 | 0.3 | 0.35
Al800 _fit | 0 | 0.09 | 0.11 | 0.12 | 0.12588 | 0.13452 | 0.15182 | 0.16986 | 0.1864 | 0.2214 | 0.26427 | 0.30795 | 0.35
G810 CERN | 0 | 0.01 | 0.02 | 0.04 | 0.048 | 0.06 | 0.063 | 0.07 | 0.076 | 0.08 | 0.09 | 0.1 | 0.12 | 0.15 | 0.2 | 0.3
G810 TRIUMF | 0 | 0.083776 | 0.083776 | 0.083776 | 0.083776 | 0.083776 | 0.084 | 0.084267 | 0.084608 | 0.085672 | 0.087778 | 0.092149 | 0.096777 | 0.10682 | 0.13659 | 0.17136 | 0.23562 | 0.32673
Chart: H, A/m
| 0 | 801 | 1197.94 | 2546.48 | 7957.75 | 15915.5 | 31831 | 48438.5 | 63662 | 95876.5 | 135336 | 175539 | 214247
Y.T. analit. | 0 | 0.05 | 0.07 | 0.08 | 0.09 | 0.1 | 0.12 | 0.14 | 0.16 | 0.2 | 0.25 | 0.3 | 0.35
Al800 _fit | 0 | 0.09 | 0.11 | 0.12 | 0.12588 | 0.13452 | 0.15182 | 0.16986 | 0.1864 | 0.2214 | 0.26427 | 0.30795 | 0.35
G810 CERN | 0 | 0.01 | 0.02 | 0.04 | 0.048 | 0.06 | 0.063 | 0.07 | 0.076 | 0.08 | 0.09 | 0.1 | 0.12 | 0.15 | 0.2 | 0.3
G810 TRIUMF | 0 | 0.083776 | 0.083776 | 0.083776 | 0.083776 | 0.083776 | 0.084 | 0.084267 | 0.084608 | 0.085672 | 0.087778 | 0.092149 | 0.096777 | 0.10682 | 0.13659 | 0.17136 | 0.23562 | 0.32673
Fitting B(H) for Al800.
Chart: I_sol, A
| 35.076999999999998 | 39.987780000000001 | 44.94867 | 50.21022 | 55.171109999999999 | 60.131999999999998 | 65.493769999999998 | 70.153999999999996 | 75.265219999999999 | 80.226109999999991 | 85.136890000000008 | 90.14788999999999 | 95.208999999999989 | 99.969450000000009
Exper. | 34 | 67 | 166 | 620 | 1261 | 1670 | 1950 | 2096 | 2180 | 2240 | 2280 | 2320 | 2350 | 2380
CST sim., dH=40 Oe | 17 | 1652
CST sim., dH=30 Oe | 18 | 32 | 114 | 1795

## Slide 10
Conclusion
Verify that ε of Al800 is constant over the 70-120 MHz interval, specify its magnitude.
Check and confirm tanδ_e=0.0002 in the 70-120 MHz interval.
Measure static B(H).
Measure unloaded Q and compare with simulations to obtain ΔH.
Start thermal simulations with new garnet parameters.