## Slide 1: On discrepancy between transmission model and 3D CST simulations
Gennady Romanov
2nd Harmonic cavity Meeting
21/V-2015

## Slide 2: Thermal losses in the transmission model
From 16April2015_2nd_Harm.ppt
Chart: μ" as a functioin of μ'
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6
Approx. formula | 3.8417e-05 | 8.1329e-05 | 0.00017217 | 0.00036449 | 0.00077163 | 0.0016335 | 0.0034582 | 0.007321 | 0.015499 | 0.03281 | 0.06946
From experiment | 0.037722 | 0.0094698 | 0.0036139 | 0.0011751 | 0.00031052
Here μ“ and μ‘ are average over garnet volume, i.e. the field non-uniformity in the so called “Thin plate” set-up is not taken into account properly.
For μ = μʹ=3.5 the model gives f = 76 MHz (start of ramp).
For tanδm = μʹʹ/μʹ = 0.000467 and voltage of 100 kV the model gives instantaneous thermal losses (Tan)
P = 62.5 kW.
According to the 3D simulations the instantaneous thermal losses at the start of ramp are
Ptotal = Pferrite + Pcopper = 12 kW + 9 kW = 21 kW
This is a big discrepancy.
A primary suspect responsible for that is non-uniformity of fields.
Lferr =( μ0 μr)/(2 π) Log[rfouter/rfinner]

## Slide 3: Thermal losses in 3D model
Garnet with fixed parameters μʹ=3.5, tanδe = 0.0001 and tanδm = 0.000467. Equivalent to transmission model
F = 75.792 MHz
Pferrite = 67 kW
Pcopper = 9 kW
Ptotal = 78 kW
Garnet with parameters obtained from “thin plate” experiment. H_ext = 35000 A/m. dH = 3.88 Oe.
Loss density
F = 78.07 MHz
Pferrite = 10.6 kW
Pcopper = 9 kW
Ptotal = 19.6 kW
Quite different loss density distribution presumes different total losses. But difference is too big to be explained by non- uniformity only. An additional factor is material properties obtained by averaging from “thin plate” experiment.

## Slide 4: Impact of non-uniformity
H_ext = 32926 gives F = 75.9 MHz. ΔH = ? Let’s assume it’s 30 Oe, then Ptotal = 40 kW.
H bias internal, 5- 32.5 kA/m
Loss density distribution, 20-1160 W/m3. Distribution of μʹ dominates.
H_rf. This distribution defines loss density in case of constant μʹ.
Distribution of μʹ, 2-19, average 3.6 (!)

## Slide 5: New material parameters
I_sol = 30 A, F = 82.48 MHz.
H internal 4500-27750 A/m
μʹ=3-14, average μʹ=5.35
Chart: Tuning curve in SteelPlug experiment
| 80.208887000000004 | 75.150099999999995 | 70.091313 | 65.1327 | 60.124000000000002 | 55.115299999999998 | 50.056513000000002 | 45.097900000000003 | 40.089199999999998 | 35.030413000000003 | 34.078760000000003 | 33.077019999999997 | 32.075279999999999 | 31.073540000000001 | 30.0718 | 29.070060000000002 | 28.06832 | 27.066579999999998
Exper. | 121.457 | 119.171 | 116.673 | 113.986 | 110.999 | 107.696 | 103.921 | 99.774 | 94.983 | 89.354 | 88.192 | 86.916 | 85.614 | 84.217 | 82.804 | 81.336 | 79.812 | 78.311
CST | 82.48 | 88.64 | 93.954 | 102.8 | 109.77 | 115.53 | 120.4 | 128.16
Chart: Damping coefficient from SteelPlug experiment
| 30 | 35 | 40 | 50 | 60 | 70 | 80
tanD_e=1e-4 | 0.0088 | 0.00354 | 0.00297 | 0.00293 | 0.00298 | 0.00313 | 0.00331
tanD_e=2e-4 | 0.00846 | 0.00308 | 0.0024 | 0.0021 | 0.00188 | 0.00173 | 0.00159
Chart: ΔH from "thin plate" and "steel plug" set ups
| 30 | 35 | 40 | 50 | 60 | 70 | 80 | 100
Steel plug | 59.15 | 23.77 | 20.15 | 20.15 | 20.15 | 20.15 | 20.15 | 20.15
Thin plate | 70 | 40 | 23 | 18 | 13 | 10 | 9 | 8

## Slide 6: Average μʹʹas a function of average μʹ
Which is right? Both are right being applied to the particular set-up.
μʹ=3-14, average μʹ=5.35
Chart: μ" as a functioin of μ'
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6
Approx. formula | 3.8417e-05 | 8.1329e-05 | 0.00017217 | 0.00036449 | 0.00077163 | 0.0016335 | 0.0034582 | 0.007321 | 0.015499 | 0.03281 | 0.06946
ThinPlate exp. | 0.037722 | 0.0094698 | 0.0036139 | 0.0011751 | 0.00031052
SteelPlug exp. | 0.00628 | 0.0015 | 0.00107 | 0.000636 | 0.000381 | 0.000284 | 0.000216 | 0.00015