## Slide 1: 2nd Harmonic Perpendicular Biased Cavity for Booster
C.Y. Tan
PIP RF cavity review
29 Sep 2015

## Slide 2: Motivation and goals
Motivation
  To improve capture efficiency in the Booster at injection.
  To improve efficiency of transition crossing.
Goal
  Build a 2nd harmonic cavity
  Use as much as possible existing RF infrastructure
    Tube Y567
      Power module
    Bias supplies
Choice of biasing
  Parallel
    Currently used in Booster
  Perpendicular
    Currently used in Recycler capture cavities (10 kHz swing)

## Slide 3: Perpendicular bias vs Parallel bias
Garnet – Al doped ferrite that contains yttrium.
Perpendicular biased garnet has higher Q than parallel bias
  Q can be a factor of 2 to 4 times higher (frequency dependent)
  Higher Q means higher gap voltage
  Higher Q means lower average power loss in garnet
Made the technical choice of doing a perpendicular biased cavity to get 100 kV in a cavity < 1 m long.
However, losses are not uniform in garnet
  Local hotspots have to be taken care of with cooling
  Location of hotspot makes cooling a challenge
Heating is the major cause of prior failures of perpendicular cavities with a large frequency swing > 10 MHz.
  Special care and feeding to make sure that this does not happen.

## Slide 4: Cavity (as of 24 Sep 2015)
Power module is modified Booster power module
Uses same Y567 tube
Beampipe ID to match 3”.
Not shown:
Window in body of cavity.
HOM damper cavity
Final solenoid design.

## Slide 5: Tuning range and proposed ramps
Reduce duty factor to 3 ms on at injection and 3 ms on at transition to mitigate any heating problems.
Duty factor 10%.
injection: 75.73 MHz
transition: 104.5 MHz
The tuning range is 30 MHz starting from 76 MHz to 106 MHz

## Slide 6: Measurement of AL800 loss tangent
Chart: ΔH(H_ext)
| 32000.0 | 35000.0 | 40000.0 | 45000.0 | 50000.0 | 55000.0 | 60000.0 | 65000.0 | 70000.0 | 75000.0 | 90000.0 | 100000.0 | 110000.0 | 120000.0 | 130000.0 | 140000.0 | 150000.0
 | 5.22 | 3.88 | 2.73 | 2.267 | 2.07 | 1.973 | 1.925 | 1.899 | 1.88 | 1.87 | 1.844 | 1.83 | 1.812 | 1.796 | 1.78 | 1.766 | 1.753
Chart: ΔH(H_ext)
| 32000.0 | 35000.0 | 40000.0 | 45000.0 | 50000.0 | 55000.0 | 60000.0 | 65000.0 | 70000.0 | 75000.0 | 90000.0 | 100000.0 | 110000.0 | 120000.0 | 130000.0 | 140000.0 | 150000.0
 | 5.22 | 3.88 | 2.73 | 2.267 | 2.07 | 1.973 | 1.925 | 1.899 | 1.88 | 1.87 | 1.844 | 1.83 | 1.812 | 1.796 | 1.78 | 1.766 | 1.753
It is critical to get the loss tangent tanδ = μ’’/μ’ correct.
I. Terechine, G. Romanov (TD) and R. Madrak (AD) spent 6 months doing both simulations and measurements to get these numbers.
These are the best measurements of AL800.
Surface magnetic flux density
300 G

## Slide 7: Thermal analyses with alumina cooling disks
Thermal conductivity
Al2O3 - 30 W/K/m
Al800 - 3.5 W/K/m
Simulation with thermal losses of P=3.2 kW and cooling water temperature of 25 °C, old ramp.
Alumina disks, 99.5%, 3 mm thickness
Water jackets
Imported distribution of thermal losses for f=74.7 MHz
T_max = 63°C
Temperature distribution
W_max = 1.13 W/cm^3
Ferrite disks,
25 mm thickness
CW

## Slide 8: Solenoid magnet (Preliminary)
Central part of the flux return is made of low-frequency high permeability ferrite; peripheral part of the flux return is assembled using silicon steel plates.
Thickness of the yoke will be optimized to avoid saturation.
Shape of the poles will be optimized for better field uniformity in the garnet material
Expected inductance of the coil is ~2.5 mH at the maximum current and ~3.5 mH at the minimum current
Expected resistive voltage is ~9 V;
Inductive voltage is ~45 V.
Existing Booster bias supplies will be able to drive this solenoid.

## Slide 9: Window locations
HFSS used to calculate surface currents, E-fields, volume losses in ceramic.
Looking at the data, this is the initial choice. This allows us to have dry nitrogen, or SF6 in garnet region to reduce multipactoring.
This choice also allows for easier assembly.

## Slide 10: Power coupler
Power coupler is capacitively coupled to the cavity.
It is strongly coupled and is part of the resonator.
  2 resonators in the system, implies that there are two normal modes.
  Must make sure that the mode that is excited in the power coupler is not close to the cavity mode.
    Separation of > 30 MHz is required to not excite the power coupler.
    Excitation in power coupler is bad because we lose power going into the accelerating mode.
    Impedance of this mode needs to be small.
Chart: Mode frequencies vs μ
| 1.5 | 2.0 | 2.5 | 3.0 | 3.5 | 4.0
Operating mode | 102.26 | 93.7656 | 86.4885 | 80.4432 | 75.406 | 71.1583
Tube mode | 129.4596 | 127.7857 | 126.8319 | 126.2028 | 125.7349 | 125.3516
Chart: Mode R_sh vs μ
| 1.5 | 2.0 | 2.5 | 3.0 | 3.5 | 4.0
Operating mode | 460.9421 | 385.83 | 336.8621 | 302.58 | 280.0139 | 263.5934
Tube mode | 49.7459 | 4.4483 | 0.79951 | 8.3601 | 19.0436 | 30.7172

## Slide 11: HOM damper
Preliminary concept done.
  Preparing for bench test of mock cavity.
Shunt impedance of fundamental reduced by 11%.
Next higher order mode reduced by 99.3%.
Everybody else between 84% to 96%. (except for 713 MHz which is small to begin with)
Load resistance is 50Ω.
Rshunt and Requiv (Ω)
HOM

## Slide 12: PA test
Y567 test to make sure that it can power cavity from 76 MHz to 106MHz.
Test stand being built
  Werlatone power combiner ordered (should be here soon)
  Solid state driver is ordered
    Bid completed
    Vendor selected.

## Slide 13: Conclusion
A lot of simulations and measurements have been done.
No show stoppers so far
  Mechanical design has started
    Some challenges as to how to assemble the garnet and the alumina and RF windows.
      Got information from CERN RF group who are also working on a 2nd harmonic cavity on how to glue garnet to alumina.
  Solenoid design has started
  Low power mock cavity is at the shop.
    Held up by shutdown priority work.
  PA test stand design nearly done
  RF components have been ordered
    Werlatone power combiner
    Solid state driver

## Slide 14: Spare slides

## Slide 15: Capture
Add in 2nd harmonic cavity to help with capture
  Flattens bucket
  Increases bucket area
ESME simulation with 10500 particles, 5e12 protons at injection with 200 MHz Linac bunch structure.
  Increase of ~2% efficiency with 100 kV 2nd harmonic cavity.

## Slide 16: Transition crossing
There is a quadrupole oscillation after transition from bucket mismatch after transition even without space charge.
Goal is to use 2nd harmonic to reduce mismatch.
One method is focus free transition crossing (FFTC).
  Note this is an example
For FFTC to work, we have to have ~200 kV 2nd harmonic voltage
  This requires 2 2nd harmonic cavities.
The idea is to flatten the RF voltage across the bunch before and after transition.
  This makes bunch “drift” with acceleration across transition.
  And an accelerating bucket with only the main RF is matched to the bunch distribution after transition.
FFTC has been demonstrated to work in Main Ring.
  Bhat et al, “Transition crossing in proton synchrotrons using a flattened rf wave”, Phys Rev E, Vol 55, Num 1, 1028-1034, 1997.