## Slide 1
Muon Production target at J-PARC
& thermal diffusivity measurements
J-PARC Center, MLF Division, Muon Section (KEK)
Shunsuke Makimura (shunsuke.makimura@kek.jp)
19th Nov. 2015
APT Seminar @FNAL
Toukai
(J-PARC)
Tsukuba
(KEK)
Tokyo

## Slide 2: Contents
Introduction of Muon Target
Fixed Target
Rotating Target
Silicon Carbide Target
~~~Break~~~
Non-destructive measurement for thermal conductivity of used muon target
Chart: Thermal conductivity
| 33 | 30 | 25 | 20 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1 | 0 | -1 | -2 | -3 | -4 | -5 | -6 | -7 | -8 | -9 | -10 | -11 | -12 | -13 | -14 | -15 | -16 | -20 | -25 | -30 | -32
horizontal | 53.267 | 52.2078 | 49.588 | 49.5874 | 45.5818 | 44.3434 | 40.9174 | 37.6662 | 31.2667 | 26.3443 | 19.9351 | 16.5304 | 15.5712 | 13.1164 | 11.9568 | 11.5673 | 12.3589 | 13.5713 | 13.546 | 14.3562 | 14.5315 | 13.3251 | 12.7959 | 12.1026 | 11.5111 | 11.3804 | 11.2015 | 11.8542 | 13.3263 | 15.7074 | 21.2865 | 27.4176 | 33.6216 | 37.9007 | 40.5178 | 42.5653 | 41.506 | 43.8629 | 46.6763 | 50.7792 | 51.7536
vertical | 58.3624 | 54.4125 | 52.2775 | 51.5265 | 51.6979 | 52.1023 | 54.2227 | 53.9717 | 53.7229 | 53.2932 | 49.7138 | 44.4957 | 36.0646 | 26.2861 | 19.2613 | 15.3494 | 13.4968 | 13.3806 | 13.8908 | 15.1894 | 14.2735 | 12.6168 | 12.2232 | 13.1951 | 16.3104 | 23.0393 | 32.7009 | 41.0128 | 47.1025 | 48.88 | 49.4502 | 48.1731 | 48.4735 | 49.0858 | 47.3416 | 47.9748 | 47.6318 | 48.4735 | 51.9282 | 55.8461 | 57.2869
Notes: When we started proton beam operation in 2008, the fixed target was installed in the beam line. Then

## Slide 3: 1. Introduction of Muon Target

## Slide 4
Japan Proton Accelerator Research Complex
(J-PARC)

## Slide 5
5
LINAC Upgrade
MR New PS
We are here
Earthquake
Hadron Acc.
New RCS schedule (undecided)
ISIS/RAL; 200kW
Fixed Target
PSI; 1MW
Rotating Target
Country | Japan | U.K. | Switzerland
Facility | J-PARC MUSE | RAL ISIS | PSI
P Intensity [MW] | 1.0(Goal) | 0.16 | 1.3
Surface Mu+ [/s] | 6 x 107(U)@0.2MW | 6 x 105 | 3 x 107
DC / Pulse | Pulse (25Hz) | Pulse (50Hz) | DC
The fixed target at J-PARC had been used for five years without replacement. The fixed target was replaced with rotating target in Sep. of 2014.

## Slide 6
Materials and Life Science Experimental Facility
& MUON TARGET
3GeV-RCS
Materials and Life Science Experimental Facility (MLF)
Neutron Target
Muon Target
The most intense pulsed muon beam all over the world
1MW in future
500kW at present

## Slide 7
Determination
of internal magnetic field distribution
H behavior
Characteristic X-ray measurement by negative muons
Magnetism and Superconductor
Positive Muon
Non-destructive Measurement
Negative Muon
Batteries Material and Hydrogen
Positvie Muon
Topics Explored by Muon
Ultra Slow Muon Generation
100 µJ
@122 nm
  ●Study Nano-science(Interfaces or multi-layered film)
  ●Surface Chemistry-Catalysis on nano-particle
Surface Muon (4 MeV, Range ~0.1mm) for BULK
Ultra Slow Muon(0.05-30 keV, Range 1 nm to ~100 nm)
Ultra Slow m+（ >105-6/s） surface muon (4×108/s)

## Slide 8: INTRODUCTION for Muon Target
Muon Target
(Graphite)
Fixed Target
Rotating Target
Proton Beam
Operation
Radioactive components
Remote controlled task in Hot cell
Muon Target System
Irradiation Damage of graphite
Post Irradiation Effect
Replacements and Checking
From RCS and BT Line
To neutron source
Muon Target
To Exp. Hall
To Exp. Hall
To Hot cell
Muon Target
System
FL1.6m
FL4m
Silicon Carbide Rotating Target

## Slide 9
Current Muon Target (Fixed Target)
Isotropic Graphite
IG-430U (Toyo Tanso)
Diameter; 70mm
Thickness; 20mm
P-Beam diameter; 16 mm (2s)
4kW heat @ 1MW proton beam
Stainless steel pipe (Water)
Copper frame
Hot Iso-static Press method
Titanium layer
as stress absorber
Silver brazing method
Journal of Nuclear Materials 377 (2008) 28-33.
70 mm
20 mm

## Slide 10
Stable Proton beam operation
Muon Target
To neutron source
Radiation dose; 750μSv/h @12 m
(150mSv/h @30cm）
Digital camera
7th July, 2014
Stable proton beam operation without replacements for 5 years
MLF beam operation; Total 15000 hours
Proton beam stop by MPS of muon target; 3 hours (Water flow Low)
No crack was observed.
 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014
Proton Beam |  |  |  |  |  |  | 
20kW Op.
Earthquake
120kW Op.
200kW Op.
Dec. 300kW
Sep.Day1
200kW Op.
300kW Op.
Hadron acc.
Replacement to Rotating Target

## Slide 11
Radiation damage of graphite
Chart: Thermal conductivity
| 33 | 30 | 25 | 20 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1 | 0 | -1 | -2 | -3 | -4 | -5 | -6 | -7 | -8 | -9 | -10 | -11 | -12 | -13 | -14 | -15 | -16 | -20 | -25 | -30 | -32
horizontal | 53.267 | 52.2078 | 49.588 | 49.5874 | 45.5818 | 44.3434 | 40.9174 | 37.6662 | 31.2667 | 26.3443 | 19.9351 | 16.5304 | 15.5712 | 13.1164 | 11.9568 | 11.5673 | 12.3589 | 13.5713 | 13.546 | 14.3562 | 14.5315 | 13.3251 | 12.7959 | 12.1026 | 11.5111 | 11.3804 | 11.2015 | 11.8542 | 13.3263 | 15.7074 | 21.2865 | 27.4176 | 33.6216 | 37.9007 | 40.5178 | 42.5653 | 41.506 | 43.8629 | 46.6763 | 50.7792 | 51.7536
vertical | 58.3624 | 54.4125 | 52.2775 | 51.5265 | 51.6979 | 52.1023 | 54.2227 | 53.9717 | 53.7229 | 53.2932 | 49.7138 | 44.4957 | 36.0646 | 26.2861 | 19.2613 | 15.3494 | 13.4968 | 13.3806 | 13.8908 | 15.1894 | 14.2735 | 12.6168 | 12.2232 | 13.1951 | 16.3104 | 23.0393 | 32.7009 | 41.0128 | 47.1025 | 48.88 | 49.4502 | 48.1731 | 48.4735 | 49.0858 | 47.3416 | 47.9748 | 47.6318 | 48.4735 | 51.9282 | 55.8461 | 57.2869
0.25dpa200℃
0.002dpa80℃
Un-irradiated
170W/m/K
Thermal conductivity
Dimensional change
Journal of Nuclear Materials 450 (2014) 110-116
Measurement of thermal conductivity for muon target at J-PARC/MUSE
1dpa
Journal of Nuclear Materials 195(1992)44-50.
graphite1991 [No.150] 290-302
Evaluation for July, 2014
Beam spot will shrink by proton irradiation.
Max. Mises stress; 30MPa
Strength; 39 MPa
New method
Laser spot heating technique
Temp. Var. by Periodic heating LD
2-D thermo-viewer

## Slide 12
Replacement of Muon Target
Residual radiation dose of muon target; 5 Sv/hour @surface
Lifetime will be less than 1 year @ 1 MW operation.
Time, Manpower, and cost are required for replacement.
Replacement in Hot cell
I must do it!!
We are eager to prolong lifetime.

## Slide 13
Rotating Target
Current fixed target
Rotating target
Proton beam
Collaboration with PSI Target group since 2004
April, 2013
Learning from Paul Scherrer Institute,
Rotating target method is applied to disperse the irradiation damage of graphite to a wider area.
The lifetime of graphite becomes long enough.
The lifetime of bearings is critical.
Solid lubricant;
Silver coating with MoS2 at PSI
Disulfide tungsten at MUSE
Expected lifetime; 10 years
E target at Paul Scherrer Institute (PSI)
Lifetime; less than 1 year

## Slide 14
Bearing & Solid lubricants
 | Type | Temp. (Kelvins) | Pressure (Pa) | Radiation | Speed (rpm) | Storage | Lifetime @15rpm (hour)
MoS2 | coating | <570 | 105 to 10-5 | general | <500 | air | 1100
Ag | coating | <600 | 10-3 to 10-10 | general | <500 | vacuum | 5800
WS2 | Separator | <600 | 105 to 10-5 | few | <210 | air | 110000
Captured from JTEKT(KOYO) Catalog
Separator made of sintered compact of WS2
Retainer, balls, & rings, coated by MoS2 or Silver
Great amount of Lubricant
Evaluation by the formula of the JTEKT Catalog
Disulfide Tungsten is used for MUSE target.
Anticipated Lifetime is 20 years!!
Radiation resistance of WS2 should be confirmed.
For our target, the bearing is used under 100 MGy/year, 400 Kelvins, 10-5 Pa

## Slide 15
Radiation Resistance of WS2
Durability tests with load & heat
4.5 million revolutions,
1year@ beam line
No irradiation effect was observed.
Electron beam irradiation
JAEA, Takasaki,
2MV, 1mA, 20hours, 100MGy

## Slide 16: Analysis of rotating target
Analysis of ordinal operation by FEM on ANSYS & Finite Difference Method on Microsoft Excel
Thermal stress ;3MPa
Maximum temp. 920 Kelvins, Difference; 80 Kelvins
Rotation speed at beam line should be 15 rpm.

## Slide 17
Mock-up of Rotating Target
Durability tests of
Target & bearings
Heating & Rotating tests
Proton beam
330 mm
Heating test
Operation for 5 days
Operation for 4 days
Motor torque (x 10 %)
9 days with 300 r.p.m. (4800h @15 r.p.m.)
It will work at least for 1 year!!

## Slide 18: Replacement of the used Fixed target
M2 line
To neutron source
M1 line
Remote-controlled camera
7th July, 2014
Radiation dose;
750μSv/h @12 m
(150mSv/h @30cm）
No crack was observed.
30th July, 2014
Dose-meter & Digital camera
FL4m
10cm gap
Transportation to tentative storage vessel
400 mSv/h @20cm

## Slide 19
Installation of Rotating Target
Rotating Target was successfully installed on 16th September of 2014.
Vacuum pressure; 10-5 Pa
Control system; Confirmed

## Slide 20: Operation of muon rotating target
Graphite temperature by thermal radiation
Cooling Jacket
Graphite wheel
Bearing
Proton beam
Horizontal shaft
Thermo-couples for shaft temp.
Trial tests for interlock in case of beam stopping
300-kW & 400-kW operation for 3 months
600-kW operations for 1 hour on 8th Apr./2015
Continuous 500-kW operation
Motor torque has been remaining constant.
 | 300kW | 500kW | 1MW
Shaft (Simulation) | 71 degC | 84 degC | 112 degC
Shaft (Measurement) | 78 degC | 95 degC | -
Graphite (Simulation) | 400 degC | 475 degC | 620 degC
Th. radiation (Measurement) | 45 degC | 60 degC | -

## Slide 21
Silicon Carbide Rotating Target for DeeMe Project
DeeMe Project;
  Muon-electron Conversion Search
  Representative; M. Aoki, Osaka University
μ- + A(Z,N) → e- +A(Z,N)
Forbidden in the Standard Model(SM) of particle physics.
No signals found yet.
Discovery of the signal → a proof of the physics beyond SM.
  Complementary to high-energy frontier experiments: LHC, ILC.
  Can explain the neutrino oscillation phenomena (Seesaw Mechanism).
r/aBohr
C nucleus
Si nucleus
μ-(C)
μ-(Si)
Graphite (C) → Si: 11-times larger overlap
μ- reaction ε: 8%(C)→67%(Si)
Silicon Carbide
Eff. of Muon Reaction: 6 times larger than C.
Hopefully, Silicon Carbide is replaced with graphite as soon as possible.
2nd Stage approval from Muon PAC of KEK/IMSS
by Aoki at Osaka Univ.

## Slide 22
Developments of Silicon Carbide Rotating Target
Comparison with graphite (Very rough discussion)
Thermal stress depends on Product of temperature (2 times) and Young’s modulus (40 times).
“Thermal stress; 80 times” VS “Strength; 10 times”
SiC has 8 times larger risk than graphite about thermal stress.
 | Density (Beam loss) | Young’s modulus | Bending Strength
Graphite (IG-430) | 1.82 g/cc (4kW) | 11 GPa | 45 MPa
SiC (SC1000, Kyocera) | 3.2 g/cc (8 kW) | 440 GPa | 450 MPa
Max. temp.; 780 degC
Preliminary heating test on Aug. 6th , 2013
Design work to reduce thermal stress

## Slide 23
SiC/SiC Composite (NITE & NIC SiC)
Possibility to introduce SiC/SiC for muon target
Advanced materials developed for nuclear & fusion reactor
by OASIS Group.
Collaboration is in progress.
FEEMA Project at OASYS
Support program at KEK (Kasokuki Shien Jigyo)
Collaboration with A. Kohyama, C. Kanda, D. Hayasaka, H. Kishimoto and Y. Kohno Organization of Advanced Sustainability Initiative for Energy System/Material (OASIS Gr.)
Muroran Institute of Technology & GUNZE Co., LTD.
High thermal conductivity (controllable)
Large and Complex Shapes
Excellent Mechanical Properties (Strength or Pseudo-ductility)
Excellent Radiation Resistance anticipated
It can be also applied for accelerator field.
1/3 model for muon target
SiC Target Collaboration

## Slide 24
Advantage of SiC with regard to Physics requirements
COMET Experiment;
Muon-Electron Conversion
Hadron Experimental Facility at J-PARC
Phase-I; 8 GeV-MR, 3.2 kW, Graphite target
Phase-II; 8 GeV-MR, 56 kW, High-Z target
Muon Transport Section is designed for Phase-II.
To reduce the disperse of muon production in the solenoid, SiC target is preferable to graphite for Phase-I.
Under discussion, with Dr. Mihara.
Pion Production Target
Capture Solenoid
These information were supplied by Dr. Mihara.
MuSIC/RCNP at Osaka Univ. by Dr. Sato
Target is also located in capture solenoid.

## Slide 25
Summary for Muon Target
Since 2008, Stable beam operation by Graphite Fixed target.
Graphite Rotating Target was installed this September.
Stable proton beam operation by Graphite Rotating target
Outline, Introduction of Muon Target
Fixed Target
Rotating Target
Silicon Carbide Target
~~~Break~~~
Non-destructive measurement for thermal conductivity of used muon target
We are here.

## Slide 26
Non-destructive measurement for thermal conductivity of used muon target
Proton Irradiation effect to thermal conductivity of graphite at J-PARC/muon target
Non-destructive measurement

## Slide 27
IG-430
Cu frame
Stainless tube
Titanium
By Kawamura
Beam profile
T. Maruyama et al., Journal of Nuclear Materials 195 (1992) 44-50.
Neutron irradiation effect to thermal conductivity
Motivation for PIE tests in our case
Lifetime; dimensional change of graphite
by proton irradiation
,which depends on the irradiated temp.
Then, How much is it?
We must guess the thermal conductivity.
The utilized data is obtained at same condition?
We hope to know actual radiation damage.
(Even if the measurement is performed in R.T.)
Domestic conditions in Muon Gr.
We are Muon Experimental Group, not Muon Target Group.
The Man-power for Muon Target is incredibly small.
No active disposal, Non-destructively
Target can be used again.
Low costs, Low man-power
But High performance

## Slide 28
Periodic heating Diode Laser
New method for this experiment
Laser Spot Heating technique
2-dimensional
thermo-meter
time
time
Temp. variation @ Heated spot
Temp. variation @distant position from heated spot
Delay of transmission; q
Non-destructively
Target can be used again.
Decreasing nucl. wastes
High spatial resolution
Comparison of Amplitude
Conventional Method
(Laser-flash technique)
time
time
Temp.@
Heated spot
Temp. @
Mating
surface
Delay of transmission
Curve of temerature rise
Cutting of specimen
Measurement
Thermal diffusivity are measured instead of Th. conductivity.
l=Drc (l; Th. Conductivity(W/m/K), D; Th. diffusivity(m2/s), r; Density (kg/m3), c; Th. Capacity (J/kg/K))
Measurement for thermal conductivity of graphite
The target must be destroyed.
We must consider transportation and the scattered radioactive powders.
The spatial resolution is limited by sample size.
(H. Kato et al., Meas. Sci. Technol. 12 (2001) 2074-2080)
Modified Thermal Imaging Scope
(Bethel. Co. LTD.)

## Slide 29
Thermal transport equation
Amplitude
q
time
time
Temp. variation @ Heated spot
Temp. variation @distant position from heated spot
Delay of transmission; q
Comparison of Amplitude
Theoretical Background of this technique
Periodic heating on Point
Pexp(iwt)
r
Carslaw H S and Jaeger J C 1959 Conduction of Heat in Solids (Oxford: Clarendon)p 263
-1
q
r
gradient
Thermo-meter
Distribution of Th. Cond. must be measured.
2-dimensional infrared thermo-meter
Expensive!!
Amplitude includes given heat by laser, P
Relative measurements based on an exact Th. Cond., obtained by other technique (Laser flash method).
Un-irradiated Th. Cond. 170W/m/K
D; Th. diffusivity(m2/s), r; Density (kg/m3), c; Th. Capacity (J/kg/K))
Evaluation by Delay
High quantitative performance
Evaluation by Amplitude
Low quantitative per., but low costs
Feasibility of Apparatus
DT; about 5 K

## Slide 30
Laser displacement meter; resolution 1mm
Laser spot heating apparatus
Shielding for radiation
mirror
The devices are set on the 3-dimensional motion stage.
Position resolution; 10mm
Indirect measurement through mirror reflection
Muon Target will set on the plug stand
Measuring Apparatus of thermal conductivity
Laser spot heating apparatus
Periodic Heating LD
2-dimensional
Thermo-meter
CCD camera
Vicinity of Muon Target; 5Sv/h, 5Gy/h for organic material (by Kawamura)
Assumption; Lifetime of measuring device, 100Gy, this means 20 hours
50mm iron shielding decreases the dose to 20 %. Extended Lifetime; 100 hours
Measurements with mirror reflection
Integrated measuring apparatus is set on a three-dimensional movable stage, which is set on plug stand.
Relative position is confirmed by laser displacement meter.

## Slide 31
Beam Profile and Anticipated Th. Conductivity
Measurement in Hot cell
Vertical
Pitch1mm
20mm x 16mm
Map pitch2mm
Horizontal
pitch1mm
If decrement of conductivity is proportional to radiation dose, the distribution for the thermal conductivity corresponds to the beam profile.
Data for IG110
From Simulation
Th. Conductivity can be anticipated,
0.25dpa on center 200degC; 5W/m/K
0.002dpa on edge 80degC; 10W/m/K
Annealing effect
The variation of thermal conductivity irradiated by neutrons
Chart: Distribution of Beam density (~RUN39)
T.Maruyama et al., Journal of Nuclear Materials 195 (1992) 44-50.
Max. 0.25dpa
0.002 dpa

## Slide 32
Chart: Thermal conductivity
| 33 | 30 | 25 | 20 | 16 | 15 | 14 | 13 | 12 | 11 | 10 | 9 | 8 | 7 | 6 | 5 | 4 | 3 | 2 | 1 | 0 | -1 | -2 | -3 | -4 | -5 | -6 | -7 | -8 | -9 | -10 | -11 | -12 | -13 | -14 | -15 | -16 | -20 | -25 | -30 | -32
horizontal | 53.267 | 52.2078 | 49.588 | 49.5874 | 45.5818 | 44.3434 | 40.9174 | 37.6662 | 31.2667 | 26.3443 | 19.9351 | 16.5304 | 15.5712 | 13.1164 | 11.9568 | 11.5673 | 12.3589 | 13.5713 | 13.546 | 14.3562 | 14.5315 | 13.3251 | 12.7959 | 12.1026 | 11.5111 | 11.3804 | 11.2015 | 11.8542 | 13.3263 | 15.7074 | 21.2865 | 27.4176 | 33.6216 | 37.9007 | 40.5178 | 42.5653 | 41.506 | 43.8629 | 46.6763 | 50.7792 | 51.7536
vertical | 58.3624 | 54.4125 | 52.2775 | 51.5265 | 51.6979 | 52.1023 | 54.2227 | 53.9717 | 53.7229 | 53.2932 | 49.7138 | 44.4957 | 36.0646 | 26.2861 | 19.2613 | 15.3494 | 13.4968 | 13.3806 | 13.8908 | 15.1894 | 14.2735 | 12.6168 | 12.2232 | 13.1951 | 16.3104 | 23.0393 | 32.7009 | 41.0128 | 47.1025 | 48.88 | 49.4502 | 48.1731 | 48.4735 | 49.0858 | 47.3416 | 47.9748 | 47.6318 | 48.4735 | 51.9282 | 55.8461 | 57.2869
Horizontal
pitch1mm
Vertical
Pitch1mm
20mm x 16mm
Map pitch2mm
We could observe an annealing effect on the center of beam spot because of high temperature.
The beam profile for horizontal/vertical could be observed.
Thermal conductivity was higher than the prediction.
0.25dpa200℃
0.002dpa80℃
Un-irradiated
170W/m/K
Chart: Total Beam Loss on Target
Results
 | Rad. Dose (dpa) | Th.Cond. Prediction | Th.Cond. Results
Center of target | 0.25 (200 degC) | 5 W/m/K | 15 W/m/K
Edge of target | 0.002 (80 degC) | 15W/m/K | 50 W/m/K
Ellipse shape

## Slide 33
20mm x 16mm
Map pitch2mm
Chart: Total Beam Loss on Target
Results
(Mapping)
Ellipse shape

## Slide 34
Summary & Future Plans
Advantages of this new technique
Non-destructively
Target can be used again.
Summary &Future Plans
Improvement of quantitative performance by meas. of q
~High speed infrared thermo-meter
We began to measure proton-irradiation damage to thermal
conductivity of graphite by brand-new laser spot heating
technique.
Measurement can be performed, non-destructively, without
contact, and with high resolution. Target can be used
again.
Distribution of thermal conductivity (relatively) can be measured successfully.
Decreasing nuclear wastes
High spatial resolution

## Slide 35
Amplitude measurement
FEM is introduced to obtain the thermal diffusivity from maximum amplitude.

## Slide 36
Quantitative performance
Reproducibility; Good (Effect of surface, scratch)
Relative measurements
Horizontal
every 5mm
Vertical
every 5mm
Chart: Distance from center (mm)
| 33 | 30 | 25 | 20 | 15 | 10 | 5 | 0 | -5 | -10 | -15 | -20 | -25 | -30 | -32
Horizontal | 170.8114 | 170.8114 | 174.6499 | 185.0457 | 171.4394 | 162.4792 | 172.072 | 176.6345 | 170.8114 | 172.7093 | 117.4597 | 168.9548 | 170.188 | 168.9548 | 145.2695
Vertical | 153.3932 | 155.9583 | 172.7093 | 163.6194 | 184.3143 | 180.7423 | 182.8687 | 178.6648 | 148.508 | 168.3448 | 165.36 | 178.6648 | 172.072 | 169.5692 | 170.188

## Slide 37
Spatial resolution
Diameter; 0.9mm
Averaged thermal conductivity

## Slide 38
Generation of Ultra Slow Muons (USM lead by Torikai)
W(2000C)
Surface Muon (4 MeV, Range ~0.1mm) for BULK
Ultra Slow Muon(0.05-30 keV, Range 1 nm to ~100 nm)
Notes: Page 23, There, J-PARC 4 MeV Surface muons are stopped in the hot W. Then towards Mu, intense lasers are introduced to ionize Mu via 1S-2P-unbound transitions.
Then Ultra Slow Muons are accelerated for the nano-meter muSR
Studies.

## Slide 39
Nature Scientific Reports SREP-13-06016-T
「A new X-ray fluorescence spectroscopy for extraterrestrial materials using a muon beam」
Non-destructive analysis by using negative muon
Comparison of Electron beam X-ray analysis and negative muon X-ray analysis. By adjusting implantation energy, composition at any depth can be obtained.
Hayabusa-Project II

## Slide 40: Isotropic Graphite
Isotropic graphite
(polycrystalline graphite)
⇔Highly Ordered Pyrolytic Graphite (HOPG)
For accelerator, nuclear reactor
Low density
High resistance to heat
Low Young’s modulus
High strength
Low residual radiation
IG-430U (Toyo Tanso); Muon Target
(IG-110; irradiation data obtained systematically)
Neutron irradiation effect to thermal conductivity
(T. Maruyama et al., Journal of Nuclear Materials 195 (1992) 44-50.)
Evaporation rate of graphite
（M.S. Avilov et al., Nuclear Instruments and Methods, A618 (2010) 1）
1mm/month
0.001mm/month
1600 degC
2000 degC
Irradiation effect to thermal conductivity

## Slide 41: Dimensional change by proton irradiation
http://www.toyotanso.co.jp/Products/Pruduct_j.pdf
HOPG (Highly Oriented Pyrolytic Graphite)
c-axis; expansion, a-axis; shrinkage (expansion > shrinkage)
(B. T. Kelly et al., Phil. Trans. A, 260 (1966) 37-49.)
Isotropic Graphite
G. B. Neighbour
Radiation damage (dpa) – Dimensional change(%)
Pore closure, Pore growth, Crystal growth
(G. B. Neighbour, J. Phys. D: Appl. Phys. 33 (2000) 2966-2972)
temp. dependence
Expansion (< 300 degC <), Shrinkage
Radiation damage (dpa)
Dimensional change (%)
No effect was observed under 2300 K without irradiation.
Proportional to rad. damage in our case. Dimensional change rate (%/dpa) depends on temperature.
Gradient; Dimensional change rate (%/dpa)

## Slide 42
Remote-controlled commissioning at Hot cell
Completed!!
To-be-installed Rotating Target
Spline nut
Coupling
Absorption of thermal expansion of the long shaft
The Others
Rotation shaft
Bearing (not fixed)
Bearing of which inner ring is fixed to shaft.
coupling
THK spline nuts DP15
Thermal expansion
Bearing of rotation F.T.
Target rod
Bevel gear for rotation of target
Top
Heavy shielding

## Slide 43
Regular maintenance for Rotating Target
Aiming lifetime; 10 years, Possibilities of break-down
1. Components, which can not be replaced easily.
Most of Bearings in vacuum & Coupling
Target itself
3. Components, which can be replaced in maintenance area (in vacuum)
Magnetic coupling FT for Rotation introduction into vacuum
Coupling. Bearing with the heaviest load
2. Components, which can be replaced in maintenance area (out of vacuum)
Motor for rotation, motor for up-down
Timing belt for up-down motion
Lifetime of some components in maintenance area; Several years (Replacement by regular maintenance)
Lifetime; > 10 years
Lifetime; 2~3years
Lifetime; 2~3years

## Slide 44
Transfer cask;
Shielding, Transport, & Gripping function
Outline of Replacement tasks
P-Beam line
Target assembly
Tentative storage vessel
FL1.6
FL4
Accessible area during beam operation
P-beam line
Target assembly
FL1.6
FL4
FL10
FL10
Transport of movable shielding
Replacement by cask
Tentative storage vessel
Preparation of new Rotating Target
Storage of used Fixed Target
Shielding
Maintenance area
Preliminary observation of the fixed target from 12-m upstream
Removal of used Fixed Target
Observation of Vicinity of the target chamber
Installation of new Rotating Target
Movable shielding
Side view
Observation from upstream
Neutron Target
FL6

## Slide 45: Preliminary observation of the used Fixed target
Photographing of the fixed target at the position of 12-m upstream by target-observation device. “Wireless Digital camera”
Alignment function & Wireless Real-time observation
No crack was observed.
M2 line
To neutron source
M1 line
Remote-controlled camera
Alignment function
7th July, 2014
Radiation dose;
750μSv/h @12 m
(150mSv/h @30cm）

## Slide 46
Removal of used Fixed Target
Transportation of Used Fixed Target from beam line to tentative storage vessel
Additional shielding was hanged to cask base.
Maintenance door is equipped on the shielding.
30th July, 2014
Dose-meter & Digital camera
Additional shielding for maintenance area
FL4m
10cm gap
Cask base
Transfer Cask
FL6m
Maintenance door

## Slide 47
Removal of used Fixed Target
Successfully, used fixed target was removed from beam line and was inserted into tentative storage vessel.
400 mSv/h @20cm
Use fixed target at tentative storage vessel
Checking of contamination
Small contamination was observed.
Transfer cask can be controlled from FL-10m.
4mSv/h
50μSv/h
15μSv/h
45μSv/h
15μSv/h
Radiation dose on the surface of transfer cask including used target
80 mSv/h
Spatial radiation dose; 6 mSv/h (Height 1m)
30th July, 2014

## Slide 48: Fabrication of Mock-up
Heating test
Horizontal shaft; 140 C
(Numerical simulation for beam line;120 C)
Rotating test; 200rpm ~500rpm
(Actual rotating speed; 15 ~ 20 r.p.m.)
Purpose
Durability tests of Bearings
Improvement for structure of the target
Development of Measuring system
Entire heating
Thermal Radiation Thermometer
Vacuum chamber

## Slide 49
Rotary Motion Feed-through,
Bevel gear, Motor
Rotary Motion Feed-through
  Anelva 954-7606, Magnetic clutch
  Maximum torque; 5.3N・m
  Allowable rotating speed; 500r.p.m.
  Cobalt Magnet, SS304, 440C stainless steel
Bevel gear
  SS440C stainless steel, without lubricant
  Load; almost 0 (N) for normal operation
  Comparison through SEM;
  After and before a long interval test
Radiation-resistant AC servo motor
  Wako-giken CO., LTD.
  Resolver Encoder
  Power output; 60W
  Torque; 0.76Nm

## Slide 50
Suppression of thermal conduction from Graphite to bearings
3 Pieces of graphite are integrated to a wheel by centrifugal rings.
Thin flat bars will absorb the thermal expansion between CF ring and outer ring of target support. They must support weight and inertia of the graphite.
Rotating Target
Chamber
Cooling jacket (Cu)
Target support
Bearing
Graphite
Items to be considered for multi-MW target
Maximum temperature of bearing, graphite
Thermal stress on graphite and the flat bars

## Slide 51
Temperature & Thermal stress by quasi-static heating on graphite (With rotation)
  Temperature difference VS Thermal stress
  on graphite
  3MPa @100 degC 10MPa @330 degC
  Limitation of temp. difference (assumption);
  330 degC
  Temp. difference;
  80 degC @1MW, 120 degC @2MW,
  280 degC @5MW
  5 MW can be accepted.
  Limitation of temp. 1600 degC
  (Evaporation rate in Vac.)
  650 degC @1MW, 840 degC @2MW,
  1150 degC @5MW
  5 MW can be accepted.
Temperature & Thermal stress on graphite
Beam spot
Diameter; 16mm
Beam loss; 3500W (1MW)
Fatigue property of IG-110
JAERI-M-84-148
Adiabatic heating by pulsed beam
  Thermal stress; 0.8MPa @1MW
  Strength; 10 MPa (assumption)
  10 MW can be accepted.
Simulation by FEM & finite difference method

## Slide 52
Thermal stress on bearing & flat bar
Temperature at bearing
  Limitation of temp. (assumption);
  Space between rings and balls; 150 degC
  By Re-design of bearing, limitation will be 300 degC.
  120 degC @1MW, 155 degC @2MW,
  235 degC@5MW
  2MW can be accepted by the current target.
  5MW can be accepted by a replaced target with re-design of bearings.
Thermal stress on flat bar
  Limitation of temp. difference(assumption);
  200MPa @350 degC, inconel strength
  110 degC @1MW, 125 degC @2MW,
  135 degC@5MW
  5MW can be accepted by the current target.
As far as the target itself is concerned, 2MW can be accepted by the current target. And 5MW can be also, with re-design of bearing.

## Slide 53: Detection of cracks
Chart: 
Cracks can be observed, through observation of diagonal thermo-couples,
①
③
⑤
⑦
left
right
Analysis of severe crack model
Max. temp.; 1480 degC
Chart: 
| 0 | 0.98615000000000008 | 1.9723000000000008 | 2.9585000000000004 | 3.9446000000000003 | 4.9308000000000014 | 5.9169 | 6.9030999999999993 | 7.8892000000000024 | 8.8754000000000062 | 9.8615000000000048 | 10.848000000000001 | 11.834000000000001 | 12.82 | 13.806000000000004 | 14.792 | 15.777999999999999 | 16.764999999999986 | 17.750999999999987 | 18.737000000000005 | 19.723000000000003
left | 47.838 | 47.127 | 46.415 | 45.829 | 45.243 | 44.741 | 44.238 | 43.799 | 43.359 | 42.969 | 42.578 | 42.23 | 41.882 | 41.567 | 41.253 | 40.967 | 40.682 | 40.432 | 40.181 | 39.989 | 39.798
right | 38.331 | 38.086 | 37.841 | 37.633 | 37.425 | 37.236 | 37.046 | 36.876 | 36.707 | 36.553 | 36.398 | 36.256 | 36.114 | 35.982 | 35.851 | 35.73 | 35.609 | 35.502 | 35.395 | 35.312 | 35.229
Temperature difference at T.C. ; 7.2 degC
It is larger than the actual temp. difference.
Actual temperature difference at T.C.@ RUN47 ; 2.2 degC
4mm offset; Beam position Down-Left
Actually, the sensitive monitoring has been achieved. The offset of the beam position can be monitored by the unbalance of the diagonal temperature .