## Slide 1: Garnet Ring Test Setup
Verification of the mechanical design per TC #F10067736

## Slide 2: Geometry
Initial proposal (July 2016)
Suggested design (Oct. 2016)

## Slide 3: 2D Modeling
1. Geometry input from the drawing in inches.
2. Garnet static permeability as we have measured.
3. Garnet RF permeability – theoretical with the measured loss coefficient α = 0.033.
4. Permittivity and dielectric loss tangent:
Garnet ε = 14 tg(δ) = 0.0001
Alumina ε = 9 tg(δ) = 0.0001
Glue (0.1 mmm) ε = 5 tg(δ) = 0.02
5. Magnetic Properties of low carbon steel 1010 (non-linear)
6. No “small 3D” design features included
Mode of oscillation
For the empty cavity:
f = 138.26 MHz
Q = 2265
CST with uniform garnet:
135.72 MHz
Q = 2154

## Slide 4: Frequency Scan
Iw = 1 kA  f = 70.626 MHz, Q = 1614
Permeability: average static – 5.94; RF – 6.38
Flux return: B_max = 0.36 T
Iw = 2.5 kA  f = 109.85 MHz, Q = 2563
Permeability: average static – 2.04; RF – 2.09
Flux return: B_max = 0.65 T
Flux return is far from being optimal
Suggested modification

## Slide 5: Updated Magnet Geometry
Magnet weight is ~40 kG now

## Slide 6: Expected Field Quality
Iw = 1 kA
Iw = 2.5 kA