## Slide 1
John Kuharik
Robyn Madrak
August 17, 2017
Garnet Ring Measurements

## Slide 2: Garnet Ring Test Stand
Measurements have been made on
Ring 1 (wrong size)
Ring 2 (chipped)
Empty cavity.

## Slide 3: First Result
Chart: Q vs f, First Garnet Measurement
| 70 | 84 | 93 | 103 | 110
Predicted | 875 | 990 | 1040 | 1080 | 1090
Measured, Garnet #2 | 675 | 800 | 1100 | 1300 | 1455 | 1460 | 670 | 520 | 1458 | 700 | 520
Measured, Garnet #1 | 595 | 840 | 1191 | 1519 | 1730 | 1800 | 850 | 612 | 855
Chart: Frequency vs Bias Current
| 4.5 | 5.7 | 6.8 | 9.1 | 11.4
Predicted | 70 | 84 | 93 | 103 | 110
Measured - Garnet #2 | 72.84 | 76 | 83.997 | 93.01 | 103 | 110 | 75.99 | 70.09 | 110.01 | 76.01 | 70.16
Measured - Garnet #1 | 69.99 | 76 | 83.999 | 92.99 | 102.999 | 110 | 75.99 | 76.01
First measurements on the rings showed a significant difference in Q between the rings and from the predicted curve.

## Slide 4: Second Measurement
The second set of measurements on Ring 1 found a small hysteresis effect by walking the bias current up and down while reversing the power leads.
Chart: Ring #1 Q vs Bias Current
| 4.7 | 5.2 | 5.9 | 7.1 | 9.3000000000000007 | 11.5
Pos up | 595 | 843 | 1200 | 1530 | 1750 | 1820
Pos down | 1820 | 1750 | 1530 | 1200 | 855 | 610 | 150
Neg down | 67 | 600 | 840 | 1200 | 1530 | 1750 | 1825
Neg up | 1825 | 1750 | 1530 | 1203 | 850 | 610 | 140
Pos up 2nd time | 63 | 600 | 850 | 1200 | 1530 | 1750 | 1820
Pos down 2nd time | 1820 | 1750 | 1535 | 1200 | 850 | 610 | 165
after "demag" | 80 | 600 | 850 | 1200 | 1535 | 1750 | 1815
The cavity was not opened between measurement 1 and this measurement.

## Slide 5: 3rd Measurement – Empty Cavity
Chart: f vs Amps - Empty Cavity
| 0 | 2 | 4.01 | 6.01 | 8 | 10 | 12 | 14 | 16.010000000000002 | 18.010000000000002 | 20.010000000000002 | 18.010000000000002 | 16 | 14 | 12 | 10 | 8 | 6 | 4 | 2.0099999999999998 | 0
f | 138.39 | 138.39 | 138.39 | 138.39 | 138.388 | 138.3869 | 138.385 | 138.383 | 138.381 | 138.379 | 138.376 | 138.377 | 138.378 | 138.379 | 138.38 | 138.382 | 138.383 | 138.383 | 138.384 | 138.384 | 138.385
Chart: Q vs Amps - Empty Cavity
| 0 | 2 | 4.01 | 6.01 | 8 | 10 | 12 | 14 | 16.010000000000002 | 18.010000000000002 | 20.010000000000002 | 18.010000000000002 | 16 | 14 | 12 | 10 | 8 | 6 | 4 | 2.0099999999999998 | 0
Q | 1292 | 1295 | 1294 | 1294 | 1295 | 1295 | 1299 | 1299 | 1296 | 1290 | 1296 | 1293 | 1293 | 1296 | 1295 | 1295 | 1294 | 1293 | 1295 | 1292 | 1294

## Slide 6: Repeatability Measurements 4-9
Chart: Q vs Bias Current Repeatability
| 4.51 | 6.5 | 8.51 | 10.5 | 12.5 | 14.5 | 16.5 | 18.5 | 20.010000000000002 | 18 | 16 | 14 | 12.01 | 10 | 8 | 6 | 4
5th Meas, Ring #1 | 393 | 1122 | 1272 | 1319 | 1324 | 1322 | 1312 | 1310 | 1310 | 1316 | 1314 | 1281 | 1307 | 1319 | 1310 | 1103 | 163
2nd Meas, Ring #1 | 595 | 843 | 1200 | 1530 | 1750 | 1820 | 1750 | 1530 | 1200 | 855 | 610 | 150
4th meas, Ring #2 | 300 | 1171 | 1440 | 1500 | 1512 | 1510 | 1497 | 1486 | 1479 | 1480 | 1493 | 1498 | 1496 | 1511 | 1440 | 1237 | 427 | 316
1st Meas, Ring #2 | 675 | 800 | 1100 | 1300 | 1455 | 1460 | 670 | 520 | 1458 | 700
'6th measurement Ring#2' | 330 | 1160 | 1310 | 1317 | 1214 | 1289 | 1284
'7th measurement Ring#2' | 350 | 1213 | 1445 | 1480 | 1486 | 1455 | 1425
'8th meas, ring #2 leads swapped' | 326 | 1240 | 1450 | 1487 | 1410
'9th meas, Ring #2, 40 in-lbs' | 410 | 1326 | 1650 | 1750 | 1774 | 1775 | 1754
Made several measurements on both rings. Best measurements of ring 1 and ring 2 match.
The difference between measurement 8 and 9 was only the torque used to tighten the cavity screws. (21 and 30 in-lbs). The cavity was not opened between them.
The new electric screwdriver with torque control was used starting with measurement 4.

## Slide 7: Repeatability Round 2
Chart: Q vs Bias Current
| 4.51 | 8.5500000000000007 | 10.49 | 14.51 | 17.739999999999998 | 20.3
Ring 2 -1 | 375 | 1694 | 1795 | 1829 | 1816 | 1807
Ring 2 -2 | 400 | 1700 | 1824 | 1846 | 1830 | 1830
Ring 2-3 | 570 | 1715 | 1791 | 1820 | 1802
Ring 1-1 | 740 | 1650 | 1751 | 1761 | 1740 | 1727
Ring 1-2 | 650 | 1694 | 1812 | 1835 | 1807
Ring 1-3 | 550 | 1645 | 1760 | 1766 | 1744 | 1724
Ring 1-4 Not tight! | 590 | 1450 | 1520 | 1512 | 1437 | 1450
5th Ring #1 Ring labeled "chip" | 393 | 1122 | 1272 | 1319 | 1324 | 1322 | 1312 | 1310 | 1310 | 1316 | 1314 | 1281 | 1307 | 1319 | 1310 | 1103 | 163
9th ring 2 | 410 | 1326 | 1650 | 1750 | 1774 | 1775 | 1754
Repeatability round two had good results. Both Rings had matching results and the best previously measured values.
One measurement had a low result due to screws not tightened properly.

## Slide 8: Empty Cavity Again, with Torque Control
Chart: Frequency and Q of Empty Cavity
| 0 | 3.57 | 7.26 | 11.8 | 14.41 | 17.760000000000002 | 20.61 | 16.920000000000002 | 13.93 | 10.11 | 7.09 | 4.24 | 0
Empty 2 f(I) | 138.658 | 138.657 | 138.657 | 138.655 | 138.655 | 138.654 | 138.652 | 138.651 | 138.651 | 138.651 | 138.651 | 138.651 | 138.651
Empty 3 f(I) | 138.625 | 138.624 | 138.624 | 138.623 | 138.623 | 138.622 | 138.621 | 138.621 | 138.62 | 138.62 | 138.62 | 138.62
Empty 1 f(I) | 138.606 | 138.606 | 138.607 | 138.607 | 138.608 | 138.609 | 138.608 | 138.608 | 138.608 | 138.608 | 138.608
Empty 2 Q(I) | 1610 | 1610 | 1619 | 1620 | 1620 | 1622 | 1625 | 1625 | 1625 | 1630 | 1630 | 1635 | 1630
Empty 3 Q(I) | 1560 | 1560 | 1570 | 1570 | 1575 | 1575 | 1570 | 1565 | 1570 | 1575 | 1575 | 1580
Empty 1 Q(I) | 1590 | 1580 | 1590 | 1585 | 1590 | 1580 | 1585 | 1580 | 1580 | 1589 | 1591

## Slide 9: Q of the empty cavity
Before the torque control screwdriver, the highest Q measured was 1400
Initially, we did an experiment to see if tightening more than 30 in lb (with the manual torque wrench) helped, and did not see an increase in Q
Now with the torque control screwdriver, Q ~ 1600
Still, all measured Q’s are substantially less than the predicted value of ~2200
Probably would be good to use the torque control screwdriver to tighten to 40 in lb and see what happens (contact effect) - No significant change found.
We will clean the cavity with Copper Brite (acid) Citrus Strip in case there is any remaining surface problem
This needs to be understood before we can be confident in our measurements of the garnet loss.