## Slide 1: The test set-up with “real’ solenoid and uniform bias.
2nd Harmonic cavity meeting
November 9, 2017
Gennady Romanov

## Slide 2: Solenoid model
Number of turns 224
Yoke
Yoke
Garnet
Ceramic
Copper
d1
d2
H
µ’=2.9÷6
I solenoid = 5 A
d1>d2, may be the garnet should be flipped over?
Lowest H ≈ 15000 A/m, while gyromagnetic resonance at 75 MHz is ≈ 2100 A/m

## Slide 3: Distribution of RF losses at I_sol = 4.2 A
Normal copper – 5.8e7 S/m
Garnet “Al800_exp4” (our base model)
Shown interval of losses is from 0.07 to 0.6 W/m3

## Slide 4: Results with constant α = 0.0036 (ΔH = 24 Oe at f0 = 9.4 GHz)
Empty
2215
1870
Frequency – excellent agreement
Q – similar general behavior
In the experiments the lowest Q is defined mostly by losses in the garnet
Gyromagnetic resonance is well below lowest internal bias field.
Non-linear α (Hbias) ?
Losses in the garnet dominate
- µ is integrated parameter, average over the disk volume, not a material characteristic.

## Slide 5: Results with fitted ΔH and two copper conductivities
“Normal copper, fitted ΔH” – ΔH was fitted to get experimental Q at low end and smoothly reach theoretical Q at high end with. Copper conductivity was kept constant (5.7e7 S/m).
“Fitted copper, fitted ΔH, uniform H” – conductivity of copper was chosen to meet experimental Q of empty test set-up and then kept constant (4.7e7 S/m), ΔH and uniform H were fitted to get experimental frequencies and Qs.
Chart: Q vs I_sol
| 4.2 | 4.9000000000000004 | 5.03 | 6.03 | 7 | 8.56 | 10.9 | 20.32
Normal copper, fitted dH | 226 | 929 | 1015 | 1591 | 1919 | 2218 | 2334 | 2279
Experiment 20171027 | 585 | 671 | 1200 | 1583 | 1870 | 2038 | 2050 | 2100 | 2091 | 2077
Fitted copper, fitted dH, uniform H | 622 | 781 | 924 | 1416 | 1716 | 1934 | 2028 | 2097 | 2074
Chart: F vs I_sol
| 4.9000000000000004 | 5.03 | 6.02 | 7 | 8.56 | 10.9 | 11.13 | 14.51 | 18.329999999999998 | 20.32 | 14.515000000000001
Experiment 20171027 | 70.985 | 73.092 | 84.3 | 91.948 | 100.116 | 107.998 | 108.698 | 115.078 | 119.447 | 121.03
Normal copper, fitted dH | 66.4 | 76.152 | 78 | 87.526 | 94.028 | 101.41 | 109.69 | 120.8
Fitted copper, fitted dH, uniform H | 70.983 | 75.551 | 78.529 | 87.8 | 94.4 | 100.58 | 105.47 | 111.2 | 113.98

## Slide 6: Non-linearity of ΔH
Chart: ΔH fitted
| 4.2 | 4.9000000000000004 | 5.03 | 6.03 | 7 | 8.56 | 10.9 | 20.32 | 14.51 | 18.329999999999998 | 20.32
Normal copper, fitted dH | 70 | 55 | 53 | 40 | 33 | 28 | 24 | 24
Fitted copper, fitted dH, uniform H | 75 | 65 | 58 | 43 | 35 | 31 | 28 | 25 | 24