## Slide 1: The 5 garnet rings
C.Y. Tan, R. Madrak & J. Kuharik
01 Feb 2018

## Slide 2: The 5 garnet rings
The 5 rings were received on 23 Jan 2018
  Arrived right on time as promised by National!
  Witness pieces did not arrive with the rings.
Robyn and Tan did a visual inspection of all the rings

## Slide 3: Visual inspection showed minor problems with 3 rings
Numbered the rings by smallest number written on the alumina substrate.
1 mm deep void in #1.
Can be easily fixed by filling with glue or grease during install.
Seam is visibly larger compared to normal seam

## Slide 4: Minor problems (#5 and #13)
#5 small voids and thicker seam.
Small excess of epoxy in #13 in one of the seams.

## Slide 5: Dimensions (manufacturer)
All dimensions within tolerance +/- 5 mils

## Slide 6: Dimensions (verification)
OD and ID measurements were done with calipers. Thickness measurements were done with micrometers.
All rings within tolerance although the scatter is a lot larger than vendor’s measurements. Need better instrument for ID measurement.

## Slide 7: Q measurements

## Slide 8: Conclusion
Rings look good.
The ”chipped” ring has been sent back to the vendor
  Still need the shim rings to be made.