## Slide 1: Accident in a cryo module
C. Baffes, M. Church, I. Rakhno
September 28, 2011

## Slide 2: Accident scenario 1: inside a cavity Electron beam (900 or 320 MeV) with 1 mm rms, hits Nb beam pipe at 1 mrad 1 pulse = 6×1013 electrons

## Slide 3: Cross section at iris

## Slide 5: Numerical data
Heat capacity of Nb at cryogenic temperatures is very small (Curtis), about 1.18 J/(kg*K) (integrated value between 2K and 9.1K). Compare to cAl = 900 J/(kg*K) at room temperature.
An estimate (Curtis) of instantaneous heating of niobium required to exceed the 9.1 K superconductivity threshold during a single 1 ms pulse: 8.4×10-7 GeV/(g*electron).
Calculated energy deposition for a number of spatial cells exceeds the value by a factor of approximately two to three orders of magnitude.

## Slide 6
Iris # Energy Deposition, GeV/(g*e-) ED/8.4×10-7
900 MeV 320 MeV 900 MeV 320 MeV
_____________________________________________________
1 1.53×10-3 1.44×10-3 1820 1710
2 1.19×10-3 5.65×10-4 1410 671
3 6.74×10-4 2.07×10-4 802 246
4 4.06×10-4 1.49×10-4 483 177
5 3.08×10-4 1.34×10-4 366 159
6 2.67×10-4 1.26×10-4 317 150
7 2.44×10-4 1.17×10-4 290 139
8 2.26×10-4 1.10×10-4 269 130

## Slide 7: Accident scenario 2: on beam pipe, just downstream of the last cavity in a cryomodule, and upstream of the following cryomodule

## Slide 9: Angle 1 mrad and beam r.m.s 1 mm mean longitudinal spread ± 100 cm 40 MeV 250 MeV

## Slide 10: Angle 1 mrad and beam r.m.s 1 mm mean longitudinal spread ± 100 cm 40 MeV 250 MeV

## Slide 11
Iris # Energy Deposition, GeV/(g*e-) ED/8.4×10-7
250 MeV 40 MeV 250 MeV 40 MeV
_____________________________________________________
1 2.93×10-5 2.39×10-5 35 28
2 7.24×10-5 2.66×10-5 86 32
3 7.41×10-5 2.42×10-5 88 29
4 6.82×10-5 2.16×10-5 81 26
5 6.10×10-5 1.91×10-5 73 23
6 5.40×10-5 1.64×10-5 64 20
7 4.69×10-5 1.42×10-5 56 17
8 4.03×10-5 1.20×10-5 48 14

## Slide 12: Conclusion
A single pulse is enough to increase the niobium temperature at multiple locations (irises) from 2 K to 9 K → quench!