2nd harmonic RF perpendicular
biased cavity update (04 Apr – 16 May 2014)
C.Y. Tan
16 May 2014

---
Agenda
- How do we want to cool the ferrite?
  - Water
  - Paraffin
  - Fluorinert
- Matching measurements of AL400 to simulations
  - The amount of demagnetization N depends on geometry!
  - Resolving the difference in μ and μ' between measurement and theory and simulations.
    - This has a bearing on the losses in the ferrite!
- Mechanical engineer. Who?

---
Cooling
- Problems with AlN is that it hydrolyzes in the presence of water.
- Get away from AlN or BeO and use direct liquid cooling
  - Water
  - Paraffin
  - Fluorinert
- The above liquids considered by KEK for their Finemet cavities.

---
Water cooling Finemet cavities
- Direct water cooling not used because of concern over material erosion and LCW contamination.
- 1” thick watercooled copper plates are used instead.
  - Electrically isolated with Kapton film between cores and copper plate.

---
Parafin cooled Finemet
- Don't need to worry about rusting
  - Flow rate is higher 1 m/s but this gives turbulent flow. (compare 0.1 m/s laminar flow for water)
  - Fire hazard? 70 degC ignition!
  - Radiation effects on parafin?
  - Electrical breakdown
    - Water 280 – 400 V/mm, parafin > 4 kV/mm

---
Fluorinert cooled Finemet
- Water causes corrosion.
  - Coatings that stop water interrupts heat transfer
    - Buckling occurs with insufficient cooling!
- Advantage of Fluorinert is that it does not contain oxygen.
  - Thermal conductivity 0.0624 W/m/K compared to water 0.628 W/m/K (10 x worse than water!)
  - Use turbulent flow to get same cooling as water in laminar flow? (page 56)
  - Must operate < 120 deg C because of ion decomposition.
  - $200 per litre!
  - ANSYS CFX to simulate flow.
    - Rudders used to remove stagnation points.
  - Flow rate 80 L/min.

---
Proposal to change ferrite geometry
- Inspiration came from demagnetization factor which is dependent on geometry of the ferrite
  - Demagnetization given by Nz 4π Ms
  - And Nz depends on geometry.
  - For annulus ID=8.661”, OD=15.354” and thickness=1”, Nz =0.74.
  - This is really a red herring because we can always overpower demagnetization with more B-field from the solenoid, especially at low field. For AL800 4πMs = 800 gauss.

---
Change cavity ferrite geometry
Reference design, volume of annuli is 742.3 cubic inches. (Nz=0.74)
We lose (742.3-544)/742.3=27% in volume.
Can make rods longer to compensate from 7.7” to 10.5” to compensate to get same volume of ferrite.
0.75” diameter rods, 7.7” long.
Shortest distance between rod surfaces 0.1”.
Total number of rods 160.
Volume of rods is 544 cubic inches.
Nz = 0.04 for 7.7” and 0.03 for 10.5” long rods

---
Advantages of rods (1)
- More surface area
  - For rods
    - (2*π*0.375)*10.5 = 24.7 sq inches per rod
    - Total surface area = 160*24.7 = 3958 sq inches.
  - For annuli
    - Each annulus has surface area
    - But there are 6 annuli, and so total surface area is 1515 sq inches < 3958 sq inches. Therefore, rods should be cooler
2 times left[%pi ( r_2^2 - r_1^2 )right] = 2 times 126 = 252.5 " sq inches"

---
Advantages of rods (2)
- Possibly cheaper to buy.
- Easier to refurbish. Just pull rods out and put in new ones.
- Can use direct water cooling if we insulate the rods with inert material. (Does ferrite corrode in the first place? Recall formula Y3Fe5O12, it's already has oxygen bonded to iron)
  - Must do this to prevent corrosion of rods.
  - Silica for insulate?
- Use sacrificial electrode like zinc????
- Expect maintenance/refurbishment schedule every 3 years?
  - Optimistic/Pessimistic?