## Slide 1: Booster 2nd harmonic cavity Loss density in ferrite
Gennady Romanov
November 11, 2014

## Slide 2
Current dimensions:
Ferrite: R = 170 mm; r = 105 mm; L = 130 mm;
L_total = 555 mm; L_coax = 355 mm; L_tuner= 200 mm; R_drift_tube = 45 mm;
R_coax = 128 mm; Aperture=70 mm (2.76”)
Yoke
Coil, 30 kA·turns max
Garnet Al800
Magnetic shielding (optional)
Water cooling
Copper cooling cylinder (optional)
Current design (no changes since last meeting)

## Slide 3
Coil length = 190 mm
Coil outer R = 283 mm
Coil inner R = 183 mm
Number of turns = 30
Model with solenoid. Volume loss density
Chart: Bias current, A
| 230 | 240 | 250 | 300 | 350 | 450 | 550 | 700 | 825 | 950
Frequency | 76.253 | 77.308 | 78.32 | 82.76 | 86.43 | 92.16 | 96.44 | 101.16 | 104.1 | 106.4
Loss density | 93.7697 | 89.2582 | 85.9098 | 69.3355 | 57.1826 | 42.1869 | 31.7197 | 22.3608 | 19.5038 | 17.0402
RF |H|-field distribution in ferrite at bias
current 230 A (µ≈3)
RF loss density distribution in ferrite at bias
current 230 A (µ≈3)
RF |H|-field distribution in ferrite at bias current 950 A (µ≈1.5)
RF loss density distribution in ferrite at bias current 950 A (µ≈1.5)

## Slide 4
Chart: Ferrite length, mm
| 130 | 120 | 110 | 100 | 90
 | 93.8 | 83.85 | 83.5 | 93 | 106.7
Chart: Ferrite length, mm
| 130 | 120 | 110 | 100 | 90
 | 405 | 481.35 | 529.5 | 561.31 | 584.46
Changes that reduce losses. The most effective is the ferrite stack length.
L_coax
Chart: Ferrite length, mm
| 130 | 120 | 110 | 100 | 90
 | 238 | 220 | 213.5 | 217 | 222
Decreasing loss density
Decreasing of ferrite length -> R_sh up, ferrite volume down, µ`` and losses up, cavity length increases.

## Slide 5
Ferrite: R=170, r=105, L=130 mm
Tuning curve with uniform bias
Chart: H_internal, Oe
| 400 | 450 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1300 | 1500 | 1700 | 1900 | 2100 | 2300 | 2500
 | 76.112 | 78.955 | 81.5 | 85.713 | 89.18 | 92.05 | 94.5 | 96.6 | 98.38 | 101.35 | 103.69 | 105.59 | 107.16 | 108.47 | 109.58
Chart: H_internal, Oe
| 400 | 450 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1300 | 1500 | 1700 | 1900 | 2100 | 2300
 | 0.55 | 0.44 | 0.37 | 0.23 | 0.13 | 0.11 | 0.14 | 0.221 | 0.301 | 0.43 | 0.524 | 0.59 | 0.63 | 0.669 | 0.701
The coupler is matched