## Slide 1: Simulation with experimental B(H).
February 17, 2015
G.Romanov

## Slide 2
Plan from February 3, 2015
Measure ε of Al800 over the 70-120 MHz interval.*
Try to check and confirm that tanδ_e=0.0002 in the 70-120 MHz interval.
Measure static B(H) of Al800 – Done (Youri&Robyn).
Measure unloaded Q in the small solenoid set-up and compare with simulations to obtain ΔH.
Start thermal simulations with new garnet parameters.
In progress
(Sergei&Youri)
* The set-up model with gaps between garnet and walls was simulated. The simulations confirmed Robyn’s conclusion about impact of the gaps on intergral ε. Fortunately average ε ≈ 10 is practically constant over the 70-120 MHz interval, so the model without gaps still can be used. Sergey was asked to take the gaps into account.

## Slide 3
Experimental B(H) for Al800.
Al800_exp2,3 – from Youri&Robyn
Chart: Experimental B(H) curves
| 0 | 1105.2427143947609 | 1829.3672514120185 | 2323.4299397495706 | 2502.4363344787039 | 3759.5657686498948 | 4591.0081982551592 | 7736.699000763324 | 10610.330058189706 | 12732.396069827648 | 18847.296813889607 | 25670.153366587991 | 39788.737718211392 | 59683.106577317092
G810_CERN | 0 | 0.01 | 0.02 | 0.04 | 0.048 | 0.06 | 0.063 | 0.07 | 0.076 | 0.08 | 0.09 | 0.1 | 0.12 | 0.15
Al800, exp_2 | 0 | 0.01 | 0.02 | 0.03 | 0.035 | 0.04 | 0.05 | 0.06 | 0.07 | 0.0816 | 0.082 | 0.085 | 0.09 | 0.095 | 0.1 | 0.11 | 0.12 | 0.13
Al800, exp_3 | 0 | 0.01 | 0.02 | 0.03 | 0.04 | 0.05 | 0.06 | 0.065 | 0.07 | 0.075 | 0.08 | 0.085 | 0.09 | 0.095 | 0.1 | 0.11 | 0.12 | 0.127 | 0.16
Chart: F(H_ext), small solenoid set-up
| 20870.841474332454 | 23792.759280738999 | 26744.492574966018 | 29875.118796115883 | 32826.852090342902 | 35778.585384569917 | 38968.842581360739 | 41741.682948664908 | 44782.862706353342 | 47734.596000580357 | 50656.513806986921 | 53638.062589034394 | 56649.426858902363 | 59481.8982018475 | 32500
Exper., H_ext=H without garnet | 73.8 | 81.65 | 87.85 | 93.633 | 98.357 | 102.457 | 106.394 | 109.428 | 112.481 | 115.163 | 117.607 | 119.914 | 122.045 | 123.917
CST sim., G810_CERN, H_ext uniform | 74.14 | 84.3 | 92.371 | 95.9 | 107.345 | 113.88 | 120.84
CST sim, Al800_exp2, H_ext uniform | 72.88 | 85.26 | 94.6 | 101.84 | 110.36 | 117.025 | 124.08

## Slide 4
Cavity mock-up (Robyn’s design).
Chart: Mock up as is, G810_CERN vs Al800_exp.
| 25000 | 30000 | 40000 | 50000 | 60000
G810_CERN | 69.945 | 75.775 | 84.41 | 90.485 | 94.75
Al800_exp | 64.34 | 72.62 | 83.06 | 89.71 | 94.43
Chart: Mock up, F vs bottom plate thickness, H_ext = 25kA/m
| 0.1 | 0.5 | 1 | 1.5
 | 78.875 | 76.463 | 74.05 | 72.35
Solenoid yoke
Copper bottom
Bottom 1.5 cm
Bottom 0.1 cm