## Slide 1: Cavity parameters used in CST, preliminary results with blocking capacitor and more thermal analyses
Gennady Romanov
2nd Harmonic cavity Meeting
1/VII-2015

## Slide 2: Definitions in CST
What are Veff, P, Rsh in CST?
Voltage Veff: CST integrates the electric field along the given voltage integration path (cavity axes typically). By definition Veff takes into account time flight factor, but currently β = 1 is assumed (β - particle relative velocity).
V/m
Thermal losses P:
Shunt impedance: Rsh = Veff2/P
FD solver -> Thermal solver

## Slide 3: FD, EM and trans. model with garnet with averaged µ´ & µ´´
Tianhuan Luo, ThinPlate data
F = 75.503 MHz
For V_peak = 100 KV:
P_ferrite_e = 8.11 kW
P_ferrite_m = 63.25 kW
P_ferrite = 71.36 kW
P_copper = 9.14 kW
P_total = 80.5 kW
The Omega3P EM simu-lation agrees well with Gennady’s results.
tanδ_m | 4.67e-4 | 2.06e-4 | 
R_sh, kΩ | 128 | 230 | CST EM
P , kW | 78 | 43.5 | 
R_sh, kΩ | 78.5 | 152 | Transmit. model
P , kW | 127.4 | 65.8 | 
For garnet with fixed parameters FD solver and
EM solver (CST and Omega3P) deliver close results.
Recalculating Tianhuan Luo results with SteelPlug tanδ = 0.000206
P_total=8.11+9.14+71.36*206/467=48.72 kW
Rsh = 100^2/48.72 = 205 kΩ
For f=76 MHz μʹ=3.5 => SteelPlug tanδ = 0.000206 (or tanδ = 0.0002145 from Tan’s approximation)
Chart: μ" as a functioin of μ'
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6
Approx. formula | 3.8417e-05 | 8.1329e-05 | 0.00017217 | 0.00036449 | 0.00077163 | 0.0016335 | 0.0034582 | 0.007321 | 0.015499 | 0.03281 | 0.06946
ThinPlate exp. | 0.037722 | 0.0094698 | 0.0036139 | 0.0011751 | 0.00031052
SteelPlug exp. | 0.00628 | 0.0015 | 0.00107 | 0.000636 | 0.000381 | 0.000284 | 0.000216 | 0.00015
R_sh, kΩ | 124 | 205 | Omega3P
P , kW | 80.5 | 48.7 | 

## Slide 4: Uniform garnet vs non-linear garnet
Losses in copper and dielectric losses:
Frequency domain solver with uniform garnet - 16.6 kW
Eigenmode solver with uniform garnet - 16.7 kW
Frequency domain with non-linear garnet at 106 MHz - 16.4 kW
Transition model at 106 MHz - 20 kW
Uniform garnet – transition model and CST eigenmode solver
Non-linear garnet – CST frequency domain with external bias
Chart: Shunt impedance vs frequency
| 106.14150166085 | 95.783935651668003 | 87.617236574019003 | 81.099097659091996 | 75.786204499058996 | 71.365940860684006 | 97.13 | 100.75 | 103.39 | 105.38 | 106.91
EM | 612 | 495 | 396 | 305 | 222.3 | 153
Trans.model | 509.416 | 467.38 | 426.789 | 387.425 | 349 | 311.7 | 275.55 | 241.06 | 208.7 | 178.86 | 151.86
FD | 236.2119 | 241.1829 | 249.9042 | 286.1559 | 352.3572 | 406.8374 | 454.13 | 507.1397 | 549.63 | 582.2581 | 608.5466
Chart: Thermal losses vs frequency
| 108.2 | 103.77200000000001 | 99.59 | 95.7 | 92.12 | 88.83 | 85.81 | 83.05 | 80.5 | 78.16 | 76
Trans.model | 19.6303 | 21.3959 | 23.4308 | 25.8114 | 28.6533 | 32.0821 | 36.2911 | 41.4834 | 47.9157 | 55.9097 | 65.8501
EM | 16.3399 | 20.202 | 25.2525 | 32.7869 | 44.9843 | 65.3595
FD | 42.3349 | 41.4623 | 40.0153 | 34.946 | 28.3803 | 24.5798 | 22.0201 | 19.7184 | 18.1941 | 17.1745 | 16.4326

## Slide 5: Power coupler or blocking capacitor
Both are overcoupled. For higher frequency the reflection is increasing.
Scaled TRIUMF coupler
Tan’s coax type blocking capacitor (L=80 mm, r = 70 mm)
Capacitance (10pF from trans. model)) is not convenient and sufficient requirement for designing. It is not even clear what is its definition in the 3D model.
E surface field

## Slide 6: Thermal analyses with alumina cooling disk
Thermal conductivity
Al2O3 - 30 W/K/m
Al800 - 3.5 W/K/m
Simulation with thermal losses of P=3.2 kW and cooling water temperature of 30 °C,
old ramp.
Alumina 99.5%, 3 mm thickness
Water jackets
Imported distribution of thermal losses for f=76.55 MHz
T_max = 85°C
Temperature distribution
Additional alumina disks will reduce T_max