Is it the best way to test parameters of a garnet specimen?

Need to make the following:

- Model fields of a cylinder sample in the magnet with different excitation coil placement.

- A sample inside a solenoid

Required magnet field in the solenoid when my = 1.5:

B = Ms + H  mu = 1 + Ms/H = 1.5  H = Ms/0.5 = 2 Ms

With Ms = 800 Oe, required H = 1600 Oe  0.16/12.5E-7 = 128000 A/m =

H*L = I  J = H = 1280 A/cm

Tuning the modeling file with I = 5 A:

- Geometry with a 5 mm gap at the coil:

- Geometry with a 2.5 mm gap at the coil:

- Geometry with a zero gap at the coil:

So, to get good results, the coil must fill all the space

How does the radial placement of the coil come in the game? Let’s use smaller current: I = 1 A

R0 = 15 mm

R = 24 mm

Practically there is no difference.

How does the permeability of the magnet core come in the game? It was 5000 Let’s make it 1000

We get smaller field due to the lower permeability of the core  a bit higher permeability of the garnet. Nevertheless, the spread did not change much – it was ~1 and now ~1.5 which seems OK.

What is we have yoke with mu = 500 ?

Spread in permeability became more significant ~6

So, material of the yoke must be good  good ferrite with mu >= 5000 or soft (1006) steel.

Let’s use mu = 1000 and go from small current to the high one and record the fields, the permeability, and the flux in the garnet.

I = 0.1 A

So, there is an increase in the field and the reduction in the permeability in the corner of the garnet  can a pole tip help ??

The field is more uniform now. Line graph is along the top portion of the garnet.

| I (A) | B_min (G) | B_max (G) | H_min (Oe) | H_max (Oe) | mu | Flux (T*m2) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.1 | 325 | 362 | 2.15 | 2.45 | 147.7 - 150 | 1.650e-5 |
| 0.15 | 453 | 493 | 3.27 | 3.76 | 131.3 – 138.2 | 2.2865e-5 |
| 0.2 | 537 | 572 | 4.42 | 5.15 | 111 – 121.5 | 2.685e-5 |
| 0.25 | 587.5 | 615 | 5.6 | 6.7 | 93.5 - 105 | 2.914e-5 |
| 0.3 | 617 | 642 | 6.7 | 9.1 | 71 - 90 | 3.034e-5 |
| 0.35 | 632.5 | 653.5 | 8.2 | 10.5 | 63 – 77.5 | 3.105e-5 |
| 0.4 | 644 | 665 | 9.3 | 11.9 | 57 - 69 | 3.16e-5 |
| 0.45 | 655 | 679 | 11.1 | 13.7 | 50 - 62 | 3.215e-5 |
| 0.5 | 665 | 687.5 | 11.8 | 15 | 45.8 – 56.7 | 3.264e-5 |
| 0.55 | 674.5 | 692.3 | 13 | 16 | 43.5 - 52 | 3.31e-5 |
| 0.6 | 682 | 699 | 14.2 | 17.3 | 40.3 – 48.3 | 3.347e-5 |
| 0.7 | 695 | 721 | 16.5 | 23.7 | 31.2 – 42.1 | 3.41e-5 |
| 0.8 | 703 | 730 | 18.7 | 27.3 | 26.9 – 38.5 | 3.46e-5 |
| 0.9 | 713 | 748 | 21 | 36.5 | 20.5 – 34.3 | 3.50e-5 |
| 1.0 | 720 | 757 | 23.2 | 40.8 | 19.5- 31 | 3.53e-5 |
| 1.5 | 743 | 797 | 34 | 60 | 13.3 – 21.8 | 3.65e-5 |
| 2.0 | 769 | 833 | 46 | 82 | 10.2 – 16.8 | 3.77e-5 |
| 2.0* | 769 | 833 | 46 | 82 | 10.2 – 16.6 | 3.78e-5 |
| 2.0** | 771 | 792 | 47 | 57.3 | 13.8 – 16.4 | 3.78e-5 |
| 5** | 866 | 896 | 109 | 142 | 6.35 – 7.92 | 4.29e-5 |
| 10** | 965 | 1055 | 212 | 287 | 3.65 – 4.61 | 4.88e-5 |
| 20** | 1180 | 1350 | 415 | 575 | 2.35 – 2.86 | 6.084e-5 |

Procedure of extracting the static permeability (B/H) is as following:

- We consider the yoke of high permeability

- Static permeability µµ0 = B/H; B = Φ/S; H = Iwcoil /L  µ = ΦL/µ0SIwcoil

- Flux Φ is found by integration of the voltage induced in the loop during current ramp around the sample (V = wloop*dΦ/dt,       Φ = 1/wloop *∫Vdt)

- So, µ = L/(µ0SIwcoilwloop)*∫Vdt

In our case, using the table above, we can find dΦ/dI  integrate it to find Φ.

We will have µ = ΦL/µ0SIwcoil

As the current increases, more spread in the field, and permeability is seen.

This is because the field from the pole is trapped in the sample:

Closer location of the coil does not change anything (see the line 2A*).

What if to make a pole profile that takes the field out of the garnet  see line 2A**

So, this profiling works well.

At 20 A near the top:

What if we use a solenoid instead of a magnet ??