Business trip: March 28&29, 2016

National Magnetics Group, Inc

NMG. TCI Ceramics

1210 Win Drive

Bethlehem, PA 18017-7061, USA

Phone: +1-610-867-6003 (x138)     Fax: +1-610-867-0200

E-mail: goutam@magneticsgroup.com

Web: www.magneticsgroup.com

To see & to ask:

- How mixes are made? How stoichiometry is controlled? How the uniformity of the mix is controlled?

- Preparation for heat processing? What is the time of firing?

- What is the furnace size and what is the temperature uniformity in the furnace?

- What is the surface quality after thing are taken from the furnace?

- How the uniformity of the properties is tested after firing? (if tested)

- What machinery and tools are used for mechanical work? What is surface quality after machining?

- What glue is used to make big assemblies? Is there any non-glue (e.g. paste) solution to use during assembly (e.g. for heat removal purpose)?

- What are major factors that define parameters of the garnet?

- What properties of the material are measured and how?

Meeting March 29, 2016

Paul Oberbeck – the owner (president)

Ph: 610 867-7600

pbo@magneticsgroup.com

Goutam Das – plant manager

Phone: +1-610-867-6003 (x138)     Fax: +1-610-867-0200

E-mail: goutam@magneticsgroup.com

Ashim Samanta – Process Engineer

Ph: 610 867-7600

ashim@magneticsgroup.com

Also presented several people that were responsible for different processes.

Talked with Ashim Samanta - overview of the processes at NMG. He promised to send his presentation file, but what I’ve got is just the titles.

Production line:

- Raw materials

- Milling

- Mixing

- Why the doping material are needed – to reduce the Ms and to change the Curie temperature.

- Drying

- Carbonizing

- Pressing and firing

- Critical steps to achieve needed properties (includes permeability, saturation magnetization, Curie temperature, thermal coefficients of permeability)

- Different processes to get the final shape (spherical powder)

- Hydrostatic pressure

- High temperature kilns

- Pressurized kiln is too small to process all the sectors for one garnet block.

- One layer layout for our work

- Mechanical shaping – very knowledgeable/enthusiastic  manager

- Possible issues with the proposed way of handling the assembly  Suggestion to make it simpler – to glue in the shop.

- Inspection of the line width of a resonance (ΔH) at 9.4 GHz

- Setup to measure the dielectric properties: ε and tg(δ) (in a cavity)

- Setup to measure hysteresis curves of the ferrite materials

- agreement to measure magnetization curve of the garnet.

- Trans-Tech flyer about the measurements of the permeability tensor.

Take a closer look:

- Nickel ferrites: NF 5000  NF5200 (4πMs = 5000 Oe  5200 Oe)

- Magnesium ferrites may provide some advantages

- M-20 material μ = 2000 and stable with T

- M3F (20) – tuner of the 10st harmonics cavity

- Alternatives for the Al garnet that reduce ΔH

- Dielectrics with different permittivity and temperature compensation !!