## Slide 1: Road to Room-Temperature Superconductivity: Superhydrides under Pressure.
Maria Baldini
APS-TD
FNAL

## Slide 2: outline
Introduction I – Pressure as a unique variable
Introduction II – Hydrogen metallization and Neil Aschroft’s predictions
Doped hydrogen – molecular compounds, hydrides and superhydrides
H3S – Conventional superconductivity at 203 K
LaHx – where all things seem to come together
Ternary systems and quest for reducing pressures
Acknowledgements

## Slide 3: Superconductivity and high pressure
SUPERCONDUCTING ELEMENTS
23 produced under pressure;
e.g., O, S, B, Fe, Li, Ca
1925: 14 years after the discovery of superconductivity. First study on Sn and Sb: Commun. Phys. Lab. Univ. Leiden 180b

## Slide 4: Superconductivity and high pressure
Pressure used to tune Tc
Highest Tc was observed at 30 GPa for many years
HgBa2Ca2Cu3O8+d
Tc = 164 K
(30 GPa)
[Gao et al., (1994); Lokshin et al. (2002)]

## Slide 5
Diamond
Graphite
P
Pressure changes everything
Carbon atoms
sp2 carbon
sp3 carbon
Pressure as a unique variable
PRESSURE
PRESSURE
Extensive mixing of orbitals valence
Volume reduction of 1.5 %
pV term in Free energy is around 10 eV
Chemical bonds drastically altered= access to a forbidden chemistry
Pressure range 0-200 GPa
Notes: Beginning of a new chemistry

## Slide 6: Range of pressure in the universe
=10 KBar
=100 GPa

## Slide 7: Pressure: Force/area
P =
F
S
1 GPa= 104 bar
P= 63 bar
Woman (63 Kg)
/ heels (1 cm2)
1 elephant (5 ton) / 1 pencil (0.5 cm2)

## Slide 8: Generating extreme pressure in the laboratory: Diamond Anvil cell (DAC)
Pressure: ambient to 400 GPa
Temperature: mK to 5000 K
Sample size < 100 um
100 GPa= 106 bar≈
1 cat (5Kg)
1 diamond (tip diameter=25 μm)
62 N
625 μm2
≈
2-4 mm
0.01-0.8 mm
1-3 mm

## Slide 9: Sample loading
2
3
4
1
Internal standard (ruby, Pt, Au)
Hydrostatic medium (NaCl, He, H2, N)
Gasket: stainless steel, Be, Re
Sample size= 80 micron
300 mm

## Slide 10: High pressure technology: Myriad of new tools
CVD
CVD

## Slide 11: outline
Introduction I – Pressure as a unique variable
Introduction II – Hydrogen metallization and Neil Aschroft’s predictions
Doped hydrogen – molecular compounds, hydrides and superhydrides
H3S – Conventional superconductivity at 203 K
LaHx – where all things seem to come together
Ternary systems and quest for reducing pressures
Acknowledgements

## Slide 12
Predicted at > 25 GPa
solid lattice of protons with delocalized electrons
Super Hydrides: Metallic Hydrogen

## Slide 13
Metallic hydrogen: A high temperature superconductor
high Debye temperature, large electron-phonon coupling, and large
density of states at the Fermi level expected for the atomic alkali-like metal system

## Slide 14
Most abundant element
Chemical dichotomy
Tests of fundamental theory
High-Tc superconductor?
Fluid ground state?
Superconducting/superfluid?
Energetic material
(400 kJ/mole: 35 x TNT)
V. L. Ginzburg was asked ”What problems of physics and astrophysics seem now to be especially important and interesting?”, Room-temperature Superconductivity
and Metallic Hydrogen appeared as number two and three on his list (Ginzburg, Key Problems in Physics and Astrophysics (1982))
Metallic hydrogen: the holy grail of high pressure science
Notes: H behave like an Halogen because of his diatomic structure, but it is often placed on the first column
Well this is actually a bigger problem and understanding hydrogen under pressure is an unsolved problem in science. It is important because it is the most abundant element.
From the standpoint of chemistry again because we think of H as a halogen, this diatomic structure, but in fact most periodic tables put it over here in this column here. So how do we think about this dichotomy of hydrogen as an alkali or a halogen? Well pressure allows us to kind of understand this by looking at the transition form the halogen form to the alkali form, at least in principal.
It is an important test of fundamental theory after all our understanding of the chemical bond started with the treatment of the H molecule. It could be a high temperature superconductor and have a fluid ground state as I have eluded to and it could have some interesting quantum properties that would make it altogether unique state of matter if one could generate this metallic form. It also contains a great amount of energy that is stored in this dense form, you have a very energetic material and understanding it as a function of pressure is also important for understanding or working on the path to inertial confinement, which is a major challenge.
We like to think of hydrogen as a fully quantum system after all one needs to also treat the electrons and the nuclei on the same footing so that gives rise to some of these interesting predicitons basically of altogether new physics of this fully quantum system in regard to the nuclei and the electrons subsystem.

## Slide 15
Metallic hydrogen: where are we now?
Metallic Hydrogen remains an unsolved problem in science.
Driven the development of high P-T techniques
Observation of the Wigner-Huntington transition to metallic hydrogen
Dias and Silvera, Science 355, 715–718 (2017)
495 GPa
Observation of a first order phase transition to metal hydrogen near 425 GPa
Paul Loubeyre, F. Occelli and P. Dumas, ArXiv June 2019
425 GPa

## Slide 16: The era of Hydrides
Use dopants in the structure?

## Slide 17
Search for new compounds: oxygen-, carbon-, sulfur-, and rare gas-bearing materials mixed with hydrogen.
H2O-H2
CH4-H2
H2S-H2
Xe-H2
New chemistry but no dissociation of molecular H2
The era of Hydrides

## Slide 18: Hydrides as high temperature superconductors
chemical precompression
H2 molecules in dense structures might be expected to dissociate at pressures well below those required for pure hydrogen
New computational structure-search methods
Density functional theory
Ab initio crystal structure prediction
Notes: of ‘chemical precompression’,
a proposal in which H2 molecules in dense structures might be expected to
dissociate at pressures well below those required for pure hydrogen. Interest in this possibility in
producing analogs of atomic metallic hydrogen was stepped up with the application of new
computational structure-search methods, which began to identify new structures with very high
predicted critical temperatures in the higher hydrides, starting with the important paper that
predicted a Tc of 235 K in CaH6.19

## Slide 19: Qualitative Guideposts for BCS Superconductivity
Bardeen-Cooper-Schrieffer (BCS) theory gives a guide for achieving high Tc and does not put bounds on Tc, all that is needed is a favorable combination of high frequency phonons (w), strong electron-phonon coupling (l), and a high density of states.
the best superconductors are covalent metals like hydrides
BCS require a metallic ground state/ covalent metals are rare at ambient conditions

## Slide 20: Qualitative Guideposts for BCS Superconductivity
large DOS at EF high phonon frequencies large electron-phonon coupling
covalent metal can be stabilized by high pressures

## Slide 21
Qualitative Guideposts for BCS Superconductivity
Extreme pressure allows to stabilize chemical
environments which would not exist spontaneously at ambient pressure (forbidden chemistry).

## Slide 22: outline
Introduction I – Pressure as a unique variable
Introduction II – Hydrogen metallization and Neil Aschroft’s predictions
Doped hydrogen – molecular compounds, hydrides and superhydrides
H3S – Conventional superconductivity at 203 K
LaHx – where all things seem to come together
Ternary systems and quest for reducing pressures
Acknowledgements

## Slide 23: Challenges in Megabar environments
Mbar pressure: samples size is 10-20 mm
H2 is dangerous for diamonds
Find a good synthesis route: pressure and Temperature
Reproducibility of the results
Sputtered electrods

## Slide 24: H3S: Tc=203 K
A.P. Drozdov, M.I. Eremets, et al. Nature 525:73–76 (2015).
Superconductive H2S: Tc∼80 K at 160 GPa
Y. Li et al. The Journal of chemical physics 140 (17) (2014) 174712.
Tc increasing with pressure > 80 K
Reproduce the result
Find a stable route
Prove superconductivity
Insulated gasket as Teflon, NaCl or CaSO4: No reaction with H2S
Ti sputtered electrodes
Sample size 25/10 um 1 um thick
Low temperature loading at 200 K: liquid H2S
Increase P afterwards.
@Max Planck Institute for Chemistry
First covalent metal hydrides was synthesized in 2008: SiHx
M. I. Eremets et al. Science:Vol. 319, Issue 5869, pp. 1506-1509

## Slide 25: H3S : Isotope effect
A.P. Drozdov, M.I. Eremets, et al. Nature 525:73–76 (2015).
Synthesis route:
Increase P at around 150 GPa
Annealing up to room T
Measuring R during cooldown and warm up
Pure sulfur
H3S experiments
H3S experiments
H3S calculation
Conventional superconductivity
Clear Isotope effect: Shift of Tc to lower temperature for D2S
D2S
H2S

## Slide 26
H3S : Magnetic field effect
Non magnetic DAC made of Cu:Ti
Tc shifts to lower values with magnetic fields
Critical field extrapolated using: Hc(T)= Hc0(1- (T/Tc)2)
Hc= 70 T with 95% confidence
Up to 7 T

## Slide 27: H3S : Magnetic field effect
H3S: cubic Im-3m
Dua et al., SCIENTIFIC REPORTS | 4, 6968 (2014)
Tc=203 K

## Slide 28: outline
Introduction I – Pressure as a unique variable
Introduction II – Hydrogen metallization and Neil Aschroft’s predictions
Doped hydrogen – molecular compounds, hydrides and superhydrides
H3S – Conventional superconductivity at 203 K
LaHx – where all things seem to come together
Ternary systems and quest for reducing pressures
Acknowledgements

## Slide 29: Superhydrides RUSh
Mishra, T. Muramatsu, H. Liu, Z. M. Geballe, M. Somayazulu, M.Ahart, M. Baldini,† Y. Meng, E. Zurek, and R.Hemley
J. Phys. Chem. C, 122, pp 19370–19378 (2018)
Ca-H system
Ca+H2 forms Ca2H5 for P < 20 GPa and T > 800 K – monoclinic phase
Ca+H2 forms CaH4 for P < 80 GPa and T > 1200 K – tI10 phase
Ca+H2 forms CaH for P ~ 120 GPa and T > 1800 K, Pm3m structure
Ca+H2 forms CaHx for P ~ 190 GPa and T > 2000 K, monoclinic phase not predicted by theory.
Relevant issues
Temperature play a critical role
find a good reproducible synthesis route
HPCAT beamline @APS Argonne National Lab.
Geophysical Lab @Carnegie Institution of Washington

## Slide 30: Synthesis and Stability of Lanthanum superhydrides
Potential high-Tc superconducting lanthanum and yttrium hydrides at high pressure
Hanyu Liu, Ivan I. Naumov, Roald Hoffmann, N. W. Ashcroft, and Russell J. Hemley
Hydrogen Clathrate Structures in Rare Earth Hydrides at High Pressures: Possible Route to Room-Temperature Superconductivity
Feng Peng, Ying Sun, Chris J. Pickard, Richard J. Needs, Qiang Wu, and Yanming Ma. Phys. Rev. Lett. 119, 107001, 2017
Super-Hydrides of Lanthanum and Yttrium: On Optimal Conditions for Achieving near Room Temperature Superconductivity. Otto, H.H. (2019) World Journal of Condensed Matter Physics 9, 22-26
Superconductivity in LaH10: A New Twist of the Story.
Kruglov, I.A., Semenok, D.V., Szcęśniak, R., Esfahani, M.M.D., Kvashnin, A.G. and Oganov, A.R. (2018) arXiv: 1810.01113
Predictions
PNAS July 3, 2017 114 (27) 6990-6995

## Slide 31: Superconductivity in LaH10-x (Synthesis)
Synthesis and Stability of Lanthanum Superhydrides
Zachary M. Geballe ,Hanyu Liu ,Ajay K. Mishra ,Muhtar Ahart, Maddury Somayazulu Yue Meng Maria Baldini , Russell J. Hemley
Angnew. Chemie, 57, 688-692 (2018)
HPCAT beamline @APS Argonne National Lab.
La
LaHx
WH
W
Au
P =170 GPa predicted phase

## Slide 32: Superconductivity in LaH10-x (Synthesis)
Synthesis and Stability of Lanthanum Superhydrides
Zachary M. Geballe ,Hanyu Liu ,Ajay K. Mishra ,Muhtar Ahart, Maddury Somayazulu Yue Meng Maria Baldini , Russell J. Hemley
Angnew. Chemie, 57, 688-692 (2018)
The synthesis has been duplicated
The P-T conditions and the synthesis of higher hydrides and decomposition products have been bracketed in the region 140-240 GPa.
H. Liu et al., Proceedings of the National Academy of Sciences 114 (27) (2017) 6990–6995.
Cubic fcc Fm3m structure
32-atom cage surrounding the rare earth atom

## Slide 33: Superconductivity in LaH10-x (validation)
Evidence for Superconductivity above 260 K in Lanthanum Superhydrides
Maddury Somayazulu, Muhtar Ahart, Ajay K. Mishra, Zachary M. Geballe, Maria Baldini,
Yue Meng, Viktor V. Struzhkin, and Russell J. Hemley
Physical Review Letter 122, 027001 (2019)
NH3BH3 ammonia borane: 3 moles of H2 an cubic BN
Pulse laser heating < 1800 K
Tc=260 K.
I>2 mA
Critical current density of 5000 A/cm2
Geophysical lab @Carnegie Institution of Washington
Notes: Pressure determined by La, Pt, Au Eos seems to be more reliable than that determined by H2 vibron or diamond Raman.

## Slide 34: Superconductivity in LaH10-x (confirmation)
Superconductivity at 250 K in Lanthanum hydride under pressure
P. Drozdov, P. P. Kong,V. S. Minkov, S. P. Besedin, M. A. Kuzovnikov, S. Mozaffari, L. Balicas, F. F. Balakirev, D. E. Graf, V. B. Prakapenka, E. Greenberg, D. A. Knyazev, M. Tkacz and M. I. Eremets
Nature, 569, 528 (2019)
Magnetic field effect
Isotopic effect: superconducting pairing mechanism
Different route
Inhomogeneities in the sample are confirmed in both experiments
Critical factor for stabilizing the phases is temperature: several phases with different Tc

## Slide 35: outline
Introduction I – Pressure as a unique variable
Introduction II – Hydrogen metallization and Neil Aschroft’s predictions
Doped hydrogen – molecular compounds, hydrides and superhydrides
H3S – Conventional superconductivity at 203 K
LaHx – where all things seem to come together
Ternary systems and quest for reducing pressures
Acknowledgements

## Slide 36: Hydrides rush
Jose A. Flores-Livasa, Lilia Boerib, Antonio Sannac, Gianni Profetad, Ryotaro Aritae, f, Mikhail Eremets, arXiv:1905.06693

## Slide 37: Future Perspective for Hydrides superconductor
Doping of binary phases
Hydrogen Energy materials: well studied at ambient conditions
Playing with metastability: several of those inaccessible phases can be stabilized at lower pressure
Example: Ternary AxByHn hydrides (gallates and alanates of alkali metals and alkaline earths) are potential candidates
Tetrahedrally coordinated at ambient conditions
Metastable octahedrally coordinated phases: metallic and superconducting phase below 100 GPa with Tc above liquid nitrogen
Jose A. Flores-Livasa, Lilia Boeri, Antonio Sannac, Gianni Profetad, Ryotaro Aritae, f, Mikhail Eremets, arXiv:1905.06693
Size of chemical landscape

## Slide 38: Conclusions
Two record breaking superconductor hydrides were discovered: H3S (2015, 200 K) and LaH10 (2018, 260 K)
Super-hydrides display conventional superconductivity
Extraordinary symbiosis between experimental search and theoretical method: effective way to find new superconductor
Room temperature superconductivity will probably be observed in coming years
Near terms: establish if conventional superconductivity can be observed in ternary, quaternary hydrides
Long terms: establish if pressure can be drastically decreased.

## Slide 39
Maddury Somayazulu
Zack Geballe
Muhtar Ahart
Ajay Mishra
Yue Meng
Hanyu Liu
Rus Hemley
Viktor Struzhkin
Takaki Muramatsu
Ivan Naumov
Changyong Park
Arun Bmmanavar
Acknowledgments
George Washington University
Geophysical lab, Carnegie Institution of Washington
HPCAT, Argonne National Lab.

## Slide 40
Acknowledgments

## Slide 43
While no dissociation is expected, the disorder in Re-H bonds under pressure causes formation of a ‘poor’ semi-metal that slowly transforms to a metal under annealing. This is paralleled in other hydride superconductors also.
Markapoulos et. al., JACS, 132, 748 (2010)
Takaki et. al., J. Phys. Chem. C, 119, 18007 (2015)
E. Vinitsky et. al. J. Phys. C, (2016)
Close, but no cigar!